# GENERAL

## SECTION INCLUDES

### Materials and installation for concrete floor hardeners, slip resistant coatings, and sheet curing materials.

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 01 51 00 - Temporary Utilities.

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

### Section 03 30 00 – Cast-in-Place Concrete.

### Section 03 35 00 - Concrete Finishing.

## REFERENCES

### Health Canada - Workplace Hazardous Materials Information System (WHMIS):

#### Safety Data Sheets (SDS).

## SUBMITTALS

### Include application instructions for concrete hardener, curing compound and slip resistant coating.

### Submit WHMIS SDS - Safety Data Sheets.

#### WHMIS SDS acceptable to Human Resources Development Canada-Labour and Health Canada for concrete floor hardeners.

#### Indicate VOC content.

## ENVIRONMENTAL REQUIREMENTS

### Temporary lighting:

#### Minimum 1200 W light source, placed 2.5 m above floor surface, for each 40 m2 of floor being finished.

### Electrical power:

#### Sufficient electrical power to operate equipment normally used during construction.

### Work area

#### Water tight protection against rain and detrimental weather conditions.

### Temperature:

#### Maintain ambient temperature of not less than 10˚C from 7 days before installation to at least 48 hours after completion of Work and maintain relative humidity not higher than 40% during same period.

#### Maintain substrate temperature at 10˚C minimum.

### Moisture:

#### Ensure concrete substrate is within moisture limits prescribed by flooring manufacturer.

### Safety:

#### Comply with requirements of Workplace Hazardous Materials Information System (WHMIS) regarding use, handling, storage, and disposal of hazardous materials.

### Ventilation:

#### Ventilate area of work as directed by Owner by use of approved portable supply and exhaust fans.

#### Ventilate enclosed spaces in accordance with Section 01 51 00 - Temporary Utilities.

#### Provide continuous ventilation during and after coating application.

# PRODUCTS

## FLOOR HARDENER

### Non-metallic hardener: premixed, aggregate type, dry shake surface hardener, cement to hardener ratio 2 to 1, cement colour.

## COLOURING AGENT

### Non-metallic type cement colouring agent, colour selected by Owner.

# EXECUTION

## EXAMINATION

### Verify that slab surfaces are acceptable for concrete hardener and curing compound application installation in accordance with manufacturer’s written instructions.

#### Visually inspect slab in presence of Owner.

#### Inform Owner of unacceptable conditions immediately upon discovery.

#### Proceed with installation only after unacceptable conditions have been remedied and after receipt of written approval to proceed from Owner.

## HARDENING

### Apply floor hardener aggregate at rate in accordance with manufacturer's written instructions

## PROTECTION

### Protect finished installation until floor treatment has completely cured.

### Repair damage to adjacent materials caused by concrete floor hardener installation.

END OF SECTION