# GENERAL

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 01 74 21 - Construction/Demolition Waste Management and Disposal.

### Section 04 05 00 - Common Work Results for Masonry.

### Section 04 05 19 - Masonry Anchorage and Reinforcing.

## REFERENCES

### American Society for Testing and Materials, (ASTM).

#### ASTM D2240, Standard Test Method for Rubber Property - Durometer Hardness.

### Canadian Standards Association (CSA)

#### CSA-A371, Masonry Construction for Buildings.

## SUBMITTALS

### Product Data:

#### Submit manufacturer's printed product literature, specifications and data including product characteristics, performance criteria, and limitations.

#### Submit two copies of WHMIS SDS - Safety Data. Indicate VOC's for joint fillers and lap adhesives.

### Manufacturer's Instructions:

#### Submit manufacturer's installation instructions.

## Delivery, Storage and Handling

### Deliver, store and handle masonry accessories in accordance with, Section 01 61 00 - Common Product Requirements supplemented as follows:

#### Keep fillers and adhesives dry, protected against dampness, and freezing.

#### Store packaged materials off ground and in accordance with manufacturer's written instructions.

# PRODUCTS

## MATERIALS

### Control joint filler: purpose-made elastomer 70 durometer hardness to ASTM D2240 of size and shape indicated. Use VOC products to limits listed in Section 01 35 21 - LEED® Requirements.

### Lap adhesive: recommended by masonry flashing manufacturer. Use VOC products to limits listed in Section 01 35 21 - LEED® Requirements.

### Weep hole vents: purpose-made PVC.

### Cavity Wall Flashing:

#### Self adhering SBS rubberized asphalt compound integrally laminated to cross-laminated polyethylene film, minimum thickness 1.0 mm.

#### Primer: as per manufacturer’s recommendation.

### Trash mortar diverters: shaped and sized to suit cavity spaces.

# EXECUTION

## MANUFACTURER'S INSTRUCTIONS

### Compliance: comply with manufacturer's written data, including product technical bulletins, product catalogue installation instructions, product carton installation instructions, and data sheets.

## INSTALLATION

### Install continuous control joint fillers in control joints at locations indicated on drawings.

### Lap adhesive: apply adhesive to flashing lap joints.

### Reglets: install reglets at locations indicated on drawings.

### Install weep hole vents in vertical joints immediately over flashings, in exterior wythes of cavity wall and masonry veneer wall construction, at maximum horizontal spacing of 600 mm on centre.

### Trash mortar diverters:  install purpose made diverters in cavities where indicated and as directed, size and shape to suit purpose and function.

## CONSTRUCTION

### Build in flashings in masonry in accordance with CSA-A371 as follows:

#### Install flashings under exterior masonry bearing on foundation walls, slabs, shelf angles, and steel angles over openings. Install flashings under weep hole courses and as indicated.

#### In cavity walls and veneered walls, carry flashings from front edge of masonry, under outer wythe, then up backing not less than 300 mm, and as follows:

##### For masonry backing embed flashing 25 mm in joint.

##### For concrete backing, insert flashing into reglets.

##### For wood frame backing, staple flashing to walls behind sheathing paper.

##### For gypsum board backing, bond to wall using manufacturer's recommended adhesive.

#### Lap joints 150 mm and seal with adhesive.

### Form flashing (end dams) at lintels, sills and wall ends to prevent water from travelling horizontally past flashing ends.

## CLEANING

### Upon completion of installation, remove surplus materials, rubbish, tools and equipment barriers.

### END OF SECTION