# GENERAL

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 04 05 00 - Common Work Results for Masonry.

### Section 04 05 12 - Masonry Mortar and Grout.

### Section 04 05 19 - Masonry Anchorage and Reinforcing.

### Section 04 05 23 - Masonry Accessories.

## REFERENCES

### American Society for Testing and Materials (ASTM)

#### ASTM E514, Standard Test Method for Water Permeance of Masonry.

#### ASTM E96, Standard Test Methods for Water Vapour Transmission of Materials.

### Canadian Standards Association (CSA)

#### CAN/CSA A165 SERIES, CSA Standards on Concrete Masonry Units, covers: A165.1, A165.2, A165.3.

#### CAN/CSA A371, Masonry Construction for Buildings.

#### CSA S304.1, Design of Masonry Structures.

### Underwriters' Laboratories of Canada (ULC).

#### CAN/ULC-S101, Standard Methods of Fire Endurance Tests of Building Construction and Materials.

## SUBMITTALS

### Product Data

#### Submit manufacturer’s printed product Literature, specifications and data sheet illustrating products to be incorporated into project for specified products.

### Samples

#### Two of each type of concrete masonry unit specified.

### Manufacturer’s Instructions

#### Submit manufacturer’s installation instructions.

### Certificates

#### Submit a certification report stating the concrete masonry unit manufacturer is in compliance with the performance and certification criteria for manufactured water-repellent concrete masonry units. Certification report to include:

##### Test method results.

##### Masonry unit physical properties.

##### Manufacturer’s certificate of performance.

## QUALITY ASSURANCE

### Mock-up

#### Construct mock-up in accordance with Section 01 45 00 – Quality Control.

#### Construct mock-up 10 m2 minimum of brick unit masonry in area designated by Owner before proceeding with brick unit masonry work.

#### Allow two (2) working days for inspection of mock-up by Owner before proceeding with Concrete Unit Masonry Work.

### Test reports:  certified test reports showing compliance with specified performance characteristics and physical properties.

### Certificates:  product certificates signed by manufacturer certifying materials comply with specified performance characteristics and criteria and physical requirements.

### Pre-installation meeting:  conduct pre-installation meeting to verify project requirements manufacturer’s instructions and manufacturer’s warranty requirements.

## QUALIFICATIONS

### Manufacturer: company specializing in manufacturing products of this section with minimum 10 years experience.

#### Hold a current certification in the manufacture of water-repellent concrete masonry units.

### Installer: company specializing in performing work of this section approved by manufacturer. Minimum 5 years experience.

### Design structural installations under direct supervision of Professional Engineer experienced in structural design of concrete masonry installation and registered in the Province of Newfoundland and Labrador.

## DELIVERY, STORAGE AND HANDLING

### Deliver, store and handle materials in accordance with Section 01 61 00 – Common Product Requirements.

### Delivery and Acceptance Requirements: deliver materials to site in original factory packaging, labelled with manufacturer’s name and address.

#### Offload concrete unit masonry packages using equipment that will not damage the surfaces.

#### Do not use brick tongs to move or handle masonry.

### Storage and Handling Requirements:

#### Store materials off ground, in dry location and in accordance with manufacturer’s recommendations in clean, dry, well-ventilated area.

#### Do not double stack cubes of concrete unit masonry.

#### Cover masonry units with non-staining waterproof membrane covering.

#### Allow air circulation around units.

#### Installation of wet or stained masonry units is prohibited.

#### Keep concrete unit masonry in individual cardboard packaging provided by manufacturer until units are ready to be installed.

#### Store and protect concrete unit masonry from nicks, scratched, and blemishes.

#### Replace defective or damaged materials with new.

# PRODUCTS

## MATERIALS

### Standard concrete block units: to CAN/CSA-A165, Series (CAN/CSA-A165.1)

#### Classification: H/10/A/M

#### Size: modular.

#### Special shapes: provide bull nosed units for exposed corners. Provide purpose-made shapes for lintels and bond beams. Provide additional special shapes as indicated.

### Split-face concrete block units Type 1: to CAN/CSA-A165 Series-04 (CSA-A165.1). Decorative face treatment: split face ashlar/centre scored.

#### Classification: S/20/A/M.

#### Size: modular as indicated on drawings.

#### Special shapes: provide square units for exposed corners. Provide purpose-made shapes for lintels and bond beams. Provide additional special shapes as indicated.

#### Colour: as selected by Owner from manufacturer’s standard colour range.

### Acoustical concrete block units: to CAN/CSA-A165 Series (CAN/CSA-A165.1) purpose made with slots to provide the acoustical characteristics specified.

#### Classification: H/10/C/M

#### Size: modular

#### Special shapes: provide special shapes indicated. Provide purpose made shapes for lintels and bond beams.

## WATER-REPELLENT ADMIXTURE

### Liquid, polymeric based water-repellent admixture to ASTM E514, incorporated into the concrete mix at block plant during the concrete masonry unit manufacturing process.

#### Water-repellent admixture to be incorporated into concrete mix at the water-repellent manufacturer’s recommended dosage.

## Accessories

### Reinforcement: to Section 04 05 19 - Masonry Anchorage and Reinforcing.

### Connectors: to Section 04 05 19 - Masonry Anchorage and Reinforcing.

### Flashing:  to Section 04 05 23 - Masonry Accessories.

### Mortar and mortar mixes: to Section 04 05 12 - Masonry Mortar and Grout.

### Grout and grout mixes: to Section 04 05 12 - Masonry Mortar and Grout.

## Cleaning Compounds

### Use VOC products to limits listed in Section 01 35 21 - LEED® Requirements.

### Compatible with substrate and acceptable to masonry manufacturer for use on products.

### Cleaning compounds compatible with concrete unit masonry and in accordance with manufacturer's written recommendations and instructions.

## Tolerances

### Tolerances for standard concrete unit masonry tolerances in accordance with CAN/CSA A165.1, supplemented as follows:

#### Maximum variation between units within specific job lot not to exceed 2.0 mm.

#### No parallel edge length, width or height dimension for individual unit to differ by more than 2.0 mm.

#### Out of square tolerance not to exceed 2.0 mm.

# EXECUTION

## INSTALLATION

### Concrete block units.

#### Bond: running

#### Coursing height: 200 mm for one block and one joint

#### Jointing: concave where exposed or where paint or other finish coating is specified

### Special Shapes:

#### Install special units to form corners, returns, offsets, reveals and indents without cut ends being exposed and without losing bond or module.

#### Install reinforced concrete block lintels over openings in masonry where steel or reinforced concrete lintels are not indicated.

#### End bearing: not less than 200 mm.

### Acoustical Concrete Unit Masonry:

#### Bond: running.

#### Coursing height: 200 mm for one block and one joint.

#### Jointing: concave where exposed or where paint or finish coating is specified.

## Construction

### Installer shall use only masonry units containing a compatible integral water-repellent admixture added to the concrete masonry units (CMU) at the time of manufacture for construction of water-repellent masonry walls.

### Installer shall use only mortar containing integral liquid polymeric water-repellent admixture at the manufacturer’s recommended addition rate and mixed according to the manufacturer’s recommended instructions for construction of water-repellent masonry walls.

### Installing Units: Use face bedding to provide the greatest resistance to water penetration.

### Cull out masonry units, in accordance with CAN/CSA A165 and approved range of color samples, with chips, cracks, broken corners, excessive color and texture variation.

### Build in miscellaneous items such as bearing plates, steel angles, bolts, anchors, inserts, sleeves and conduits.

### Construct masonry walls using running bond unless otherwise noted.

### Fit masonry closely against electrical and plumbing outlets so collars, plates and covers overlap and conceal cuts.

### Install movement joints and keep free of mortar where indicated.

### Hollow Units: spread mortar setting bed from outside edge of face shells.  Gauge amount of mortar on top and end of unit to create full joints, equivalent to shell thickness. Avoid excess mortar.

### Solid Units: apply mortar over entire vertical and horizontal surfaces. Avoid bridging of airspace between brick veneer and backup wall with mortar.

### Ensure compacted head joints. Use full or face-shell joint as indicated.

### Tamp units firmly into place.

### Do not adjust masonry units after mortar has set.  Where resetting of masonry is required, remove, clean and reset units in new mortar.

### Tool exposed joints concave; strike concealed joints flush.

### After mortar has achieved initial set up, tool joints.

### Do not interrupt bond below or above openings.

## CLEANING

### Promptly remove excess wet mortar containing integral water-repellent mortar admixture from face of masonry as work progresses by dry brushing.

### Clean masonry once mortar is set and cured.

### Upon completion of installation remove surplus materials, rubbish, tools and equipment barriers.

## Protection

### Brace and protect concrete unit masonry in accordance with Section 04 05 00 - Common Work Results for Masonry.

### Cover top of unfinished masonry work to protect it from the weather and to prevent accumulation of water in CMU cores.

### END OF SECTION