# General

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 01 61 00 - Common Product requirements.

### Section 01 74 21 - Construction/Demolition Waste Management and Disposal.

### Section 03 30 00 - Cast-in-Place Concrete.

### Section 04 05 00 - Common Work Results for Masonry.

### Section 04 05 19 - Masonry Anchorage and Reinforcing.

### Section 05 12 23 - Structural Steel for Buildings.

### Section 05 21 00 - Steel Joist Framing.

### Section 05 31 00 - Steel Decking.

### Section 05 51 00 - Metal Stairs and Ladders.

### Section 09 91 13 - Exterior Painting.

### Section 09 91 23 - Interior Painting.

## REFERENCES

### American Society for Testing and Materials, (ASTM)

#### ASTM A53/A53M, Specification for Pipe, Steel, Black and Hot-Dipped, Zinc-Coated Welded and Steamless.

#### ASTM A269, Specification for Seamless and Welded Austenitic Stainless Steel Tubing for General Service.

#### ASTM A307, Specification for Carbon Steel Bolts and Studs, 60,000 PSI Tensile Strength.

### Canadian General Standards Board (CGSB)

#### CAN/CGSB 1.153, High-Build, Gloss Epoxy Coating.

### Canadian Standards Association (CSA)

#### CAN/CSA-G40.20/G40.21, General Requirements for Rolled or Welded Structural Quality Steel.

#### CAN/CSA-G164, Hot Dip Galvanizing of Irregularly Shaped Articles.

#### CSA S16, Design of Steel Structures.

#### CSA W48, Filler Metals and Allied Materials for Metal Arc Welding (Developed in co-operation with the Canadian Welding Bureau).

#### CSA W59, Welded Steel Construction (Metal Arc Welding).

### The Environmental Choice Program

#### CCD-047, Architectural Surface Coatings.

#### CCD-048, Surface Coatings - Recycled Water-borne.

### Green Seal Environmental Standards (GS)

#### GS-11, Paints and Coatings.

### The Master Painters Institute (MPI)

#### Architectural Painting Specification Manual.

## SUBMITTALS

### Product Data:

#### Submit manufacturer's printed product literature, specifications and data sheet

#### Submit two copies of WHMIS SDS - Safety Data Sheets. Indicate VOC's:

##### For finishes, coatings, primers and paints.

### Shop Drawings

#### Indicate materials, core thicknesses, finishes, connections, joints, method of anchorage, number of anchors, supports, reinforcement, details, and accessories.

## QUALITY ASSURANCE

### Test Reports: Submit Certified test reports showing compliance with specified performance characteristics and physical properties.

### Certificates: Submit Product certificates signed by manufacturer certifying materials comply with specified performance characteristics and criteria and physical requirements.

## DELIVERY, STORAGE, AND HANDLING

### Deliver, store, handle and protect materials in accordance with Section 01 61 00 - Common Product Requirements.

### Cover exposed stainless steel surfaces with pressure sensitive heavy protection paper or apply strippable plastic coating, before shipping to job site.

### Leave protective covering in place until final cleaning of building. Provide instructions for removal of protective covering.

# Products

## MATERIALS

### Steel sections and plates: to CAN/CSA-G40.20/G40.21, Grade 300W.

### Steel pipe: to ASTM A53/A53M standard weight, galvanized finish.

### Welding materials: to CSA W59.

### Welding electrodes: to CSA W48 Series.

### Bolts and anchor bolts: to ASTM A307.

### Grout: non-shrink, non-metallic, flowable, 15 MPa at 24 hours.

## FABRICATION

### Fabricate work square, true, straight and accurate to required size, with joints closely fitted and properly secured.

### Use self-tapping shake-proof flat round oval headed screws on items requiring assembly by screws or as indicated.

### Where possible, fit and shop assemble work, ready for erection.

### Ensure exposed welds are continuous for length of each joint. File or grind exposed welds smooth and flush.

## FINISHES

### Galvanizing: hot dipped galvanizing with zinc coating 600 g/m2 to CAN/CSA-G164.

#### Optional Finish for exterior steel angle lintels: stainless steel to ASTM A276, S304.

### Shop coat primer: in accordance with chemical component limits and restrictions requirements and VOC limits of GS-11.

### Zinc primer: zinc rich, ready mix: in accordance with chemical component limits and restrictions requirements and VOC limits of GS-11.

### High Build Epoxy Coating:  to CAN/CGAB – 1.153.

## ISOLATION COATING

### Isolate aluminum from following components, by means of bituminous paint:

#### Dissimilar metals except stainless steel, zinc, or white bronze of small area.

#### Concrete, mortar and masonry.

#### Wood.

## SHOP PAINTING

### Apply one shop coat of primer to metal items, with exception of galvanized or concrete encased items.

### Use primer unadulterated, as prepared by manufacturer. Paint on dry surfaces, free from rust, scale, grease. Do not paint when temperature is lower than 7 degrees C.

### Clean surfaces to be field welded; do not paint.

## ANGLE LINTELS

### Steel angles: galvanized prime painted sizes indicated for openings. Provide 150 mm minimum bearing at ends.

#### Optional stainless steel finish for exterior steel angle lintels.

### Weld or bolt back-to-back angles to profiles as indicated.

### For non stainless steel angle lintels, apply one shop coat of primer and finish to Section 09 91 13 – Exterior Painting.

## PIPE RAILINGS

### Steel pipe: 30 to 40 mm nominal outside diameter for handrails. For other handrails, formed to shapes and sizes as indicated.

### Shop coat prime interior railings after fabrication.  Apply high build epoxy coating after fabrication.  Shop coat prime exterior railings after fabrication and finish to Section 09 91 13 – Exterior Painting.

## ACCESS LADDERS INTERIOR/EXTERIOR

### Design Access Ladders to OHS Standards for Stage Access.

### Stringers: 55 x 55 x 6 mm thick, steel angle.

### Steel Rungs: 20 mm diameter, welded to stringers at 300 mm on centre.

### Brackets: sizes and shapes as indicated, weld to stringers at 1200 mm c.c., complete with fixing anchors.

### Shop coat prime interior ladders after fabrication.  Shop coat prime exterior ladders after fabrication and apply a high build epoxy coating finish to Section 09 91 13 – Exterior Painting.

## TRENCH COVERS AND FRAMES

### Fabricate from 6 mm thick steel set in L 55 x 55 x 6 frame. Include anchors at 1200 mm on centre for embedding in concrete. Supply trench covers in 1200 mm removable lengths.

### Finish: galvanized.

### Paint as per Section 09 91 13 – Exterior Painting.

## CHANNEL FRAMES

### Fabricate frames from steel, sizes of channel and opening as indicated.

### Weld channels together to form continuous frame for jambs and head of openings, sizes as indicated.

### Shop coat prime interior channel frames after fabrication.  Shop coat prime exterior channel frames after fabrication and apply a high build epoxy coating finish Section 09 91 13 – Exterior Painting.

# Execution

## ERECTION

### Do welding work in accordance with CSA W59 unless specified otherwise.

### Erect metalwork square, plumb, straight, and true, accurately fitted, with tight joints and intersections.

### Provide suitable means of anchorage acceptable to Owner such as dowels, anchor clips, bar anchors, expansion bolts and shields, and toggles.

### Exposed fastening devices to match finish and be compatible with material through which they pass.

### Provide components for building by other sections in accordance with shop drawings and schedule.

### Make field connections with bolts to CAN/CSA-S16, or weld.

### Hand items over for casting into concrete or building into masonry to appropriate trades together with setting templates.

### Touch-up rivets, field welds, bolts and burnt or scratched surfaces after completion of erection with primer.

### Touch-up galvanized surfaces with zinc rich primer where burned by field welding.

### Touch-up high build epoxy coated finishes.

## PIPE RAILINGS

### Install pipe railings to stairs as indicated.

### Set railing standards in concrete. Grout to fill hole. Trowel surface smooth and flush with adjacent surfaces.

## ACCESS LADDERS

### Install access ladders in locations as indicated.

### Erect ladders 200mm clear of wall on bracket supports.

## TRENCH COVERS

### Install trench covers in locations as indicated.

## CHANNEL FRAMES

### Install steel channel frames to openings as indicated.

## CLEANING

### Perform cleaning after installation to remove construction and accumulated environmental dirt.

### Upon completion of installation, remove surplus materials, rubbish, tools and equipment barriers.

## PROTECTION

### Protect installed products and components from damage during construction.

### Repair damage to adjacent materials caused by metal fabrications installation

END OF SECTION