# GENERAL

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

## REFERENCES

### American Wood-Preservers' Association (AWPA)

#### AWPA M2, Standard Inspection of Treated Wood Products.

#### AWPA M4, Standard for the Care of Preservative-Treated Wood Products.

### Canadian Standards Association (CSA)

#### CSA O80 Series, Wood Preservation.

#### CSA O322, Procedure for Certification of Pressure-Treated Wood Materials for Use in Preserved Wood Foundations.

### Underwriters Laboratory of Canada (ULC)

#### CAN/ULC-S102 Surface Burning Characteristics of Building Materials and Assemblies.

## REGULATORY REQUIREMENTS

### Each board or bundle of fire-retardant treated material panel to bear ULC label indicating Flame Spread Classification (FSC), and smoke developed.

## CERTIFICATES

### For products treated with preservative, fire-retardant by pressure impregnation submit following information certified by authorized signing officer of treatment plant:

#### Information listed in AWPA M2 and revisions specified in CSA O80 Series, Supplementary Requirement to AWPA M2 applicable to specified treatment.

#### Moisture content after drying following treatment with water-borne preservative, fire-retardant.

#### Acceptable types of paint, stain, and clear finishes that may be used over treated materials to be finished after treatment.

## WASTE MANAGEMENT AND DISPOSAL

### Do not dispose of preservative treated wood through incineration.

### Do not dispose of preservative treated wood with other materials destined for recycling or reuse.

### Dispose of treated wood, end pieces, wood scraps and sawdust at sanitary landfill approved by Owner.

### Dispose of unused wood preservative material at official hazardous material collections site approved by Owner.

### Do not dispose of unused preservative material into sewer system, into streams, lakes, onto ground or in other location where they will pose health or environmental hazard.

# PRODUCTS

## MATERIALS

### Preservative: to CAN/CSA-O80 Series, stained finish.

### Fire-Retardant: to CAN/CSA O80.20.

### Solvent: to CAN/CSA-O80.201.

# EXECUTION

## APPLICATION: PRESERVATIVE

### Treat lumber to CAN/CSA- O80 Series.

### Following water-borne preservative treatment, dry material to maximum moisture content of 19%.

## APPLICATION: FIRE-RETARDANT

### Treat lumber by pressure impregnation with fire-retardant chemicals in accordance with CAN/CSA - O80.20.

### Following treatment, kiln-dry material to maximum moisture content of 19%.

## APPLICATION: FIELD TREATMENT

### Comply with AWPA M4 and revisions specified in CAN/CSA-O80 Series, Supplementary Requirements to AWPA Standard M2.

### Treat all field cuts with two (2) coats of clear copper napthenate or 5% pentachlorophenol solution, water repellent preservative.

### Remove chemical deposits on treated wood to receive applied finish.

END OF SECTION