# GENERAL

## RELATED SECTIONS

### Section 01 74 21 - Construction/Demolition Waste Management and Disposal.

### Section 06 05 73 - Wood Treatment.

### Section 06 17 53 - Shop-Fabricated Wood Trusses.

### Section 07 52 00 - Modified Bituminous Membrane Roofing

### Section 07 92 00 - Joint Sealants.

### Section 09 21 16 - Gypsum Board Assemblies.

## REFERENCES

### American Society for Testing and Materials (ASTM)

#### ASTM A123/A123M, Standard Specification for Zinc (Hot-Dip Galvanized) Coatings on Iron and Steel Products.

#### ASTM A653/A653M, Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process.

#### ASTM C578, Specification for Rigid, Cellular Polystyrene Thermal Insulation.

#### ASTM C1396/C1396M, Standard Specification for Gypsum Board.

#### ASTM D5055, Specification for Establishing and Monitoring Structural Capacities of Prefabricated Wood I-Joists.

#### ASTM F1667, Standard Specification for Driven Fasteners: Nails, Spikes and Staples.

### Canadian General Standards Board (CGSB)

#### CAN/CGSB-71.26, Adhesive for Field-Gluing Plywood to Lumber Framing for Floor Systems.

### Canadian Wood Council

#### Wood Design Manual.

#### Engineering Guide for Wood Frame Construction.

### Canadian Standards Association (CSA)

#### CSA A123.2, Asphalt Coated Roofing Sheets.

#### CSA B111, Wire Nails, Spikes and Staples.

#### CSA 0112.9, Evaluation of Adhesives for Structural Wood Products (Exterior Exposure).

#### CSA O121, Douglas Fir Plywood.

#### CSA-O141, Softwood Lumber.

#### CSA O151, Canadian Softwood Plywood.

#### CSA-O325.0, Construction Sheathing.

### National Lumber Grades Authority (NLGA)

#### Standard Grading Rules for Canadian Lumber.

### National Research Council Canada (NRC)

#### National Building Code of Canada (NBC).

## QUALITY ASSURANCE

### Lumber identification: by grade stamp of an agency certified by Canadian Lumber Standards Accreditation Board.

### Plywood, particleboard, OSB and wood based composite panels in accordance with CSA and ANSI standards.

## ACTION AND INFORMATIONAL SUBMITTALS

### Submit in accordance with Section 01 33 00- Submittal Procedures.

### Submit proof of compatibility between Alkaline Copper Quaternary (ACQ) pressure treated lumber and fasteners to be utilized.

### Product Data:

#### Submit manufacturer's instructions, printed product literature and data sheets for wood products and accessories and include product characteristics, performance criteria, physical size, finish and limitations.

#### Include manufacturer’s pre-engineered floor, ceiling and roof joist span charts, and manufacturer’s pre-engineered installation details.

#### Submit certified test reports for prefabricated structural members from approved independent laboratory indicating compliance with specifications for specified performance characteristics and physical properties.

#### Submit CCMC Product Evaluation Report for engineered wood products.

#### Submit manufacturer’s installation instructions.

### Shop Drawings:

#### For structural applications or conditions beyond the scope of the manufacturer’s pre-engineered design information, submit drawings stamped and signed by professional engineer registered or licensed in the Province of Newfoundland and Labrador.

#### Include on drawings:

##### Design data in accordance with CAN/CSA-O86 and CWC Engineering Guide for Wood Frame Construction.

##### Indicate configuration and spacing of joists, hanger and connector types, fasteners, locations and design values; bearing details.

##### Submit stress diagrams or print out of computer design indicating design loads for members. Indicate allowable load and stress increase.

##### Indicate arrangement of webs or other members to accommodate ducts and other specialties

## DELIVERY, STORAGE, AND HANDLING

### Deliver, store and handle materials in accordance with Section 01 61 00- Common Product Requirements.

### Delivery and Acceptance Requirements: deliver materials to site in original factory packaging, labelled with manufacturer's name and address.

### Storage and Handling Requirements:

#### Store materials in dry location, off ground and in accordance with manufacturer's recommendations in clean, dry, well-ventilated area.

#### Store materials off ground with moisture barrier at both ground level and as a cover forming a well-ventilated enclosure, with drainage to prevent standing water.

#### Store wood I-beams and I-joists on edge.

#### Stack, lift, brace, cut and notch engineered lumber products in strict accordance with manufacturer’s instructions and recommendations.

#### Store and protect architecturally exposed lumber from[nicks, scratches, and blemishes.

#### Replace defective or damaged materials with new.

#### Store separated reusable wood waste convenient to cutting station and work areas.

# PRODUCTS

## STRUCTURAL FRAMING

### Lumber: unless specified otherwise, softwood, No. 1 or No. 2 grade, S4S, moisture content 19% (S-dry) or less in accordance with following standards:

#### CAN/CSA-O141.

#### NLGA Standard Grading Rules for Canadian Lumber.

### Wood I-joists in accordance with Prefabricated Wood I-Joists ASTM D5055.

### Framing and board lumber: in accordance with NBC.

### Furring, blocking, nailing strips, grounds, rough bucks, fascia backing and sleepers:

#### Board sizes: "Standard" or better grade.

#### Dimension sizes: "Standard" light framing or better grade.

#### Post and timbers sizes: "Standard" or better grade.

### Pressure treated material to be Alkaline Copper Quaternary (ACQ).

### Where indicated, provide pressure treated materials for furring, blocking, nailing strips, grounds, rough bucks, cants, curbs, fascia backing and sleepers in accordance with Section 06 05 73.

## PANEL MATERIALS

### Plywood, OSB and wood based composite panels: to CAN/CSA-O325.0.

### Douglas fir plywood (DFP): to CSA O121, standard construction.

### Canadian softwood plywood (CSP): to CSA O151, standard construction.

### Insulating fiberboard sheathing: to CAN/CSA-A247.

### Expanded polystyrene sheathing: to Section 07 21 13 – Board Insulation.

### Gypsum sheathing: to 09 21 16 – Gypsum Board Assemblies.

## ACCESSORIES

### Exterior wall sheathing paper: to CAN/CGSB-51.32 single ply, spunbonded olefin type coated impregnated as indicated.

### Polyethylene film: to Section 07 26 00 – Vapour Retarders.

### Sill Gasket Air seal: closed cell polyurethane or polyethylene.

### Sealants: Section 07 92 00 – Joint Sealants.

### General purpose adhesive: to CSA O112.9.

### Nails, spikes and staples: to CSA B111.

### Bolts: 12.5 mm diameter unless indicated otherwise, complete with nuts and washers.

### Proprietary fasteners: toggle bolts, expansion shields and lag bolts, screws and lead or inorganic fibre plugs, explosive actuated fastening devices, recommended for purpose by manufacturer.

### Joist hangers: minimum 1 mm thick sheet steel, galvanized ZF001 coating designation.

### Roof sheathing H-Clips: formed "H" shape, thickness to suit panel material, type approved by Owner.

## FASTENER FINISHES

### Galvanizing: to ASTM A123/A123M, ASTM A653, use galvanized fasteners for exterior work, interior highly humid areas and fire-retardant treated lumber.

## WOOD PRESERVATIVE

### Surface-applied wood preservative: clear or copper napthenate or 5% pentachlorophenol solution, water repellent preservative.

# EXECUTION

## PREPARATION

### Treat surfaces of material with wood preservative, before installation.

### Apply preservative by dipping, or by brush to completely saturate and maintain wet film on surface for minimum 3 minute soak on lumber and one minute soak on plywood.

### Re-treat surfaces exposed by cutting, trimming or boring with liberal brush application of preservative before installation.

### Treat all material as indicated as follows:

#### Wood fascia, backing, curbs, nailers.

#### Wood furring for sheeting/siding on outside surface of exterior masonry concrete walls.

#### Wood sleepers supporting wood subflooring over concrete slabs in contact with ground or fill.

## SYSTEMS INTEGRATION

### Install air barrier and vapour retarder sheeting around framing members to ensure continuity of protection and to lap and seal to main sheets.

### Install insulation in exterior wall framing cavities that will not be accessible after completion of framing.

### Install sill plate gasket in continuous lengths between concrete surfaces and wood framing.

## INSTALLATION

### Comply with requirements of NBC latest edition, Part 9 supplemented by following paragraphs.

### Install members true to line, levels and elevations, square and plumb.

### Construct continuous members from pieces of longest practical length.

### Install spanning members with "crown-edge" up.

### Select exposed framing for appearance. Install lumber and panel materials so that grade-marks and other defacing marks are concealed or are removed by sanding where materials are left exposed.

### Frame, anchor, fasten, tie and brace members to provide necessary strength and rigidity.

### Countersink bolts where necessary to provide clearance for other work.

### Install specified panel product for each application.

### Install subflooring and combined subfloor and underlay with panel end-joints located on solid bearing, staggered at least 800 mm.

#### In addition to mechanical fasteners, apply subflooring adhesive under panels installed on wood joints. Place continuous adhesive bead in accordance with manufacturer's instructions, single-bead on each joist and double-bead on joists where panel ends butt.

#### Use decking screws for mechanical fasteners when weather conditions are unsuitable for subflooring adhesive.

### Install wall sheathing in accordance with manufacturer's printed instructions.

### Install roof sheathing in accordance with requirements of NBC.

### Install furring and blocking as required to space-out and support casework, cabinets, wall and ceiling finishes, facings, fascia, soffit, siding electrical equipment mounting boards, and other work as required.

### Install furring to support siding applied vertically where there is no blocking and where sheathing is not suitable for direct nailing.

#### Align and plumb faces of furring and blocking to tolerance of 1:600.

### Install rough bucks, nailers and linings to rough openings as required to provide backing for frames and other work.

### Install wood cants, fascia backing, nailers, curbs and other wood supports as required and secure using galvanized steel fasteners. Coordinate height of roof curbs with Section 07 52 00 – Modified Bituminous Membrane Roofing.

### Install sleepers as indicated.

### Use dust collectors and high quality respirator masks when cutting or sanding wood panels.

## SCHEDULES

### Roof sheathing:

#### Plywood, DFP or CSP sheathing grade (SHG) T&G edge, 16 mm thick, unless otherwise indicated.

### Exterior wall sheathing:

#### Plywood, DFP or CSP sheathing grade or (SHG) grade, T&G edge, 16 mm thick, unless otherwise indicated.

#### Expanded polystyrene sheathing, Type 1, RSI indicated, shiplapped edges, thickness as indicated.

#### Gypsum sheathing, Section 09 21 16 – Gypsum Board Assemblies.

### Subflooring:

#### Plywood, DFP or CSP sheathing grade (SHG) T&G edge, 19 mm thick, unless otherwise indicated.

### Electrical equipment mounting boards:

#### Plywood, DFP or CSP grade, (G1S) select square edge 16 mm thick, unless otherwise indicated.

### Underlay:

#### Plywood, DFP or CSP sheathing grade (Select), square edge 6 mm thick, unless otherwise indicated.

## PROTECTION

### Protect installed products and components from damage during construction.

### Repair damage to adjacent materials caused by rough carpentry installation.

END OF SECTION