# GENERAL

## RELATED SECTIONS

### Section 01 29 83 - Payment Procedures for Testing Laboratory Services.

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

### Section 06 05 73 - Wood Treatment.

### Section 06 10 53 – Miscellaneous Rough Carpentry.

## REFERENCES

### Canadian Standards Association (CSA)

#### CSA B111, Wire Nails, Spikes and Staples.

#### CAN/CSA O80 Series, Wood Preservation.

#### CSA O86, Engineering Design in Wood.

### National Lumber Grades Authority

#### NLGA Standard Grading Rules for Canadian Lumber.

## QUALITY ASSURANCE

### Lumber identification: by grade stamp of an agency certified by Canadian Lumber Standards Accreditation Board.

# PRODUCTS

## MATERIALS

### Wood decking: to NLGA standard Grading Rules for Canadian Lumber Select grade Spruce 38 mm, predrilled at 750mm o.c. for lateral spiking, single tongue and groove and "Veed" one side. Kiln dry decking to 15% maximum moisture content.

### Decking lengths: 1.8 to 6.0 m or longer with a minimum of 90% planks exceeding 3.0 m. square end trimmed. For single spans shorter than 3.0 m use decking of same length as span.

### Nails: to CSA B111, hot dipped galvanized finish; sizes as recommended in CAN/CSA-O86. Supply 200 mm spiral spikes for lateral nailing.

### Splines: galvanized metal, as recommended by decking manufacturer.

### Wood preservative: water borne type to CAN/CSA O80.

# EXECUTION

## INSTALLATION

### Do wood deck work in accordance with CAN/CSA O86 except where specified otherwise.

### Install decking in accordance with CAN/CSA O86, simple span pattern.

### Provide minimum of one bearing support for each plank.

### Stagger end joints in adjacent planks minimum of 0.5 m. Separate joints in same area by at least two intervening courses. Avoid joints in first fifth of end spans. Minimize joints in middle third of any span.

### Touch up end cuts with preservative where pressure treated lumber is specified.

## FIELD QUALITY CONTROL

### Testing moisture content of delivered material will be performed by testing laboratory designated by Owner.

### Owner will pay for costs of testing as specified in Section 01 29 83- Payment Procedure for Testing Laboratory Procedures.

## CLEANING

### Remove tool marks, bruises, and scratches.

## FINISH

### Refer to Exterior Painting Section 09 91 13.

## PROTECTION

### Protect installed products and components from damage during construction.

### Repair damage to adjacent materials caused by wood decking installation.

END OF SECTION