# GENERAL

## SECTION INCLUDES

### Materials and installation for asphalt for use as dampproofing.

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 01 51 00 - Temporary Utilities.

### Section 01 61 00 - Common Product Requirements.

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

## REFERENCES

### Canadian General Standards Board (CGSB)

#### CAN/CGSB 37.2, Emulsified Asphalt, Mineral-Colloid Type, Unfilled, for Dampproofing and Waterproofing and for Roof Coatings.

#### CAN/CGSB 37.3, Application of Emulsified Asphalts for Dampproofing or Waterproofing.

#### CAN/CGSB 37.5, Cutback Asphalt Plastic Cement.

#### CGSB 37-GP-9Ma, Primer, Asphalt, Unfilled, for Asphalt Roofing, Dampproofing and Waterproofing.

#### CGSB 37-GP-11M, Application of Cutback Asphalt Plastic Cement.

#### CAN/CGSB 37.16, Filled, Cutback, Asphalt for Damproofing and Waterproofing.

#### CGSB 37-GP-36M, Application for Filled Cutback Asphalts for Damproofing and Waterproofing.

### National Research Council Canada (NRC)/Institute for Research in Construction (IRC)

#### Canadian Construction Materials Centre (CCMC)

## PRODUCT DATA

### Submit product data sheets for bituminous dampproofing products. Including:

#### Product characteristics.

#### Performance criteria.

#### Application methods.

#### Limitations.

### Manufacturer's Instructions: Provide to indicate special handling criteria, installation sequence, cleaning procedures.

## DELIVERY, STORAGE AND HANDLING

### Deliver, handle, store and protect materials of this section in accordance with Section 01 61 00 - Common Product Requirements.

### Provide and maintain dry, off-ground weatherproof storage.

### Store materials on supports to prevent deformation.

### Remove only in quantities required for same day use.

### Store materials in accordance with manufacturer's written instructions.

## PROJECT/SITE ENVIRONMENTAL REQUIREMENTS

### Temperature, relative humidity, moisture content.

#### Apply dampproofing materials only when surfaces and ambient temperatures are within manufacturers' prescribed limits.

#### Do not proceed with Work when wind chill effect would tend to set bitumen before proper curing takes place.

#### Maintain air temperature and substrate temperature at dampproofing installation area above 5˚C for 24 hours before, during and 24 hours after installation.

#### Do not apply dampproofing in wet weather.

### Safety: Comply with requirements of Workplace Hazardous Materials Information System (WHMIS) regarding use, handling, storage, and disposal of asphalt, sealing compounds, primers and caulking materials.

### Ventilation:

#### Ventilate enclosed spaces in accordance with Section 01 51 00 - Temporary Utilities.

#### Provide continuous ventilation during and after dampproofing application. Run ventilation system 24 hours per day during installation; provide continuous Ventilation for 3 days after completion of dampproofing installation.

# Products

## MATERIALS

### For application and curing at temperatures above 5° C: waterproof emulsion, mineral colloid emulsifier type to CAN/CGSB 37.2.

#### Package label or bill of lading for bulk hot liquid asphalt must indicate type, flash point, equiviscous temperature range and final blowing temperature.

### For applications and curing at temperatures above 0° C but below 5° C: solvent type waterproofing and dampproofing compound of selected asphalts and fibers to CAN/CGSB 37.16.

#### Package label or bill of lading for bulk hot liquid asphalt must indicate type, flash point, equiviscous temperature range and final blowing temperature.

### Primer for applications at temperatures above 0° C but below 5° C: asphalt/solvent cutback to CAN/CGSB 37.9.

### Sealing compound:  plastic cutback asphalt cement to CAN/CGSB-37.5. C.

# EXECUTION

## WORKMANSHIP

### Keep hot asphalt:

#### Below its flash point.

#### At or below its final blowing temperature.

#### Within its equiviscous temperature range at place of application.

## PREPARATION

### Before applying dampproofing:

#### Seal exterior joints between foundation walls and footings, joints between concrete floor slab and foundation and around penetrations through dampproofing with sealing compound.

## APPLICATION

### Do dampproofing in accordance with CAN/CGSB 37.3 and CGSB 37-GP-36M except where specified otherwise.

### Do sealing work in accordance with CGSB 37-GP-11M except where specified otherwise.

### Do priming of surface in accordance with CGSB 37-GP-15M except where specified otherwise.

### Apply primer.

## SCHEDULE

### Apply continuous, uniform coating to entire exterior faces of foundation walls from 50 mm below finished grade level to and including tops of foundation wall footings.

### Apply continuous, uniform coating to exterior side of foundation walls enclosing rooms below finished grade. Include exterior portion of interior walls where floors in adjacent rooms are at different elevations.

### Apply two additional coats of dampproofing to vertical corners and construction joints for a minimum width of 230 mm on each side, and all around and for 230 mm along pipes passing through walls.

END OF SECTION