NL Master Specification Guide

for Public Funded Buildings
Re-Issued 2017/05/31
Section 07 21 16 –Blanket Insulation
Page 2 of 3

Part 1 GENERAL

1.1 RELATED SECTIONS
.1 Section 01 33 00 - Submittal Procedures.

.2 Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

.3 Section 06 10 53 – Miscellaneous Rough Carpentry.

.4 Section 07 26 00 - Vapour Retarders.

1.2 REFERENCES

.1 American Society for Testing and Materials, (ASTM).

.1 ASTM C553, Specification for Mineral Fibre Blanket Thermal Insulation for Commercial and Industrial Applications.

.2 ASTM C665, Specification for Mineral-Fiber Blanket Thermal Insulation for Light Frame Construction and Manufactured Housing.

.3 ASTM C1320, Standard Practice for Installation of Mineral Fiber Batt and Blanket Thermal Insulation for Light Frame Construction.

.4 ASTM E84, Test Method for Surface Burning Characteristics of Building Materials.

.2 Canadian Standards Association (CSA International).

.1 CSA B111, Wire Nails, Spikes and Staples.

.2 CSA B149 PACKAGE, Consists of B149.1, Natural Gas and Propane Installation Code and B149.2, Propane Storage and Handling Code.

.3 Underwriters Laboratories of Canada (ULC).

.1 CAN/ULC-S702, Standard for Mineral Fibre Insulation.

1.3 SUBMITTALS
.1 Product Data:

.1 Submit manufacturer's printed product literature, specifications and data sheet.

.2 Manufacturer's Instructions:

.1 Submit manufacturer's installation instructions.

Part 2 PRODUCTS
2.1 INSULATION
.1 Thermal batt and blanket mineral fibre: 
.1 Unfaced glass fiber thermal insulation to ASTM C665 Type I, thickness and RSI value as indicated on drawings.

.2 Semi-rigid mineral wool batt insulation to CSA/ULC-S702, made from basalt rock and slag, thickness and RSI value as indicated on drawings.

.2 Acoustic batt insulation:

.1 Unfaced glass fiber acoustical insulation to ASTM C665, Type I, thickness as indicated.

.1 Flame spread: 10 to ASTM E84.

.2 Smoke development: 10 to ATSM E84.

.3 Sound transmission Class: STC 49.

.4 Dimensional stability: linear shrinkage less than 0.1%.

Part 3 EXECUTION

3.1 MANUFACTURER’S INSTRUCTIONS

.1 Compliance: comply with manufacturer’s written data, including product technical bulletins, product catalogue installation instructions, product carton installation instructions, and data sheets.

3.2 INSULATION INSTALLATION
.1 Install insulation to maintain continuity of thermal protection to building elements and spaces and for sound attenuation as noted on drawings.

.2 Fit insulation closely around electrical boxes, pipes, ducts, frames and other objects in or passing through insulation.

.3 Do not compress insulation to fit into spaces.

.4 Keep insulation minimum 75 mm from heat emitting devices such as recessed light fixtures, and minimum 50 mm from sidewalls and CSA B149.1 and CSA B149.2 Type B and L vents.

.5 Do not enclose insulation until it has been inspected and approved by Owner.

3.3 CLEANING
.1 Upon completion of installation, remove surplus materials, rubbish, tools and equipment barriers.

END OF SECTION
Ver. 10/22

