# GENERAL

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 01 74 21 - Construction/Demolition Waste Management and Disposal.

### Section 01 45 00 - Quality Control.

### Section 01 51 00 - Temporary Utilities.

### Section 07 26 00 –Vapour Retarders

### Section 07 27 00.01 – Air Barriers - Descriptive or Proprietary.

## REFERENCES

### Canadian Urethane Foam Contractors' Association Inc. (CUFCA)

### Underwriters' Laboratories of Canada (ULC)

#### CAN/ULC-S101, Fire Endurance Tests of Building Construction and Materials.

#### CAN/ULC-S102, Surface Burning Characteristics of Building Materials and Assemblies.

#### CAN/ULC-S705.1, Standard for Thermal Insulation Spray Applied Rigid Foam, Medium Density, Material Specification.

#### CAN/ULC-S705.2, Standard for Thermal Insulation Spray Applied Rigid Foam, Medium Density, Installer's Responsibilities-Specification.

## TEST REPORTS

### Submit test reports, verifying qualities of foam sealant meet or exceed requirements of this specification.

### Submit test reports in accordance with CAN/ULC-S101 for fire endurance and CAN/ULC-S102 for surface burning characteristics.

## QUALITY ASSURANCE

### Applicators to conform to CUFCA Quality Assurance Program.

## SAFETY REQUIREMENTS

### Protect workers as recommended by CAN/ULC-S705.2 and manufacturer's recommendations:

#### Workers must wear gloves, respirators, dust masks, eye protection, protective clothing when applying foam sealant.

#### Workers must not eat, drink or smoke while applying foam sealant.

## PROTECTION

### Ventilate area in accordance with Section 01 51 00 - Temporary Utilities.

### Ventilate area to receive insulation by introducing fresh air and exhausting air continuously during and 24 hours after application to maintain non-toxic, unpolluted, safe working conditions.

### Provide temporary enclosures to prevent spray and noxious vapours from contaminating air beyond application area.

### Protect adjacent surfaces and equipment from damage by overspray, fall-out, and dusting of insulation materials.

### Dispose of waste foam sealant daily in location designated by Owner and decontaminate empty drums in accordance with foam sealant manufacturer’s instructions.

## ENVIRONMENTAL REQUIREMENTS

### Apply foam sealant only when surfaces and ambient temperatures are within manufacturers' prescribed limits.

# PRODUCTS

## MATERIALS

### Low expanding, one-component, polyurethane foam sealant, curing to a semi-rigid, closed cell urethane foam providing a RSI of 0.9 per 25.4 mm. To meet the following physical properties:

#### Density:					25.7 kg/m3

#### Compressive Strength Parallel @ 10%:	69-96 psi

#### Tensile Strength:				103 psi

#### Water Vapour Transmission:		5.97 perms

#### Flame Spread:				20

#### Smoke Development:			70

# EXECUTION

## APPLICATION

### Apply foam sealant to clean surfaces in accordance manufacturer's printed instructions. Surfaces to be free of dust, dirt, oil and other foreign materials.

### Cover surfaces not intended to be foamed.

### Apply foam sealant to perimeter of openings indicated and to thickness as recommended by manufacturer. Trim excess cured foam from finished area.

### Cover exposed urethane foam sealants to protect from adverse affects from ultraviolet light (sunlight).

END OF SECTION