# GENERAL

## RELATED SECTIONS

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

### Section 01 43 39 – Mock Up Requirements.

### Section 01 45 00 - Quality Control.

### Section 01 51 00 - Temporary Utilities.

### Section 07 26 00 –Vapour Retarders.

### Section 07 27 00.01 – Air Barriers - Descriptive or Proprietary.

## REFERENCES

### ASTM International (ASTM)

#### ASTM C1029, Standard Specification for Spray-Applied Rigid Cellular Polyurethane Thermal Insulation.

### Canadian Urethane Foam Contractors' Association Inc. (CUFCA)

### Underwriters' Laboratories of Canada (ULC)

#### CAN/ULC-S102, Surface Burning Characteristics of Building Materials and Assemblies.

#### CAN/ULC-S705.1, Standard for Thermal Insulation - Spray Applied Rigid Polyurethane Foam, Medium Density, Material Specification. Includes Amendment 1.2.

#### CAN/ULC-S705.2, Standard for Thermal Insulation - Spray Applied Rigid Polyurethane Foam, Medium Density, Application.

## SUBMITTALS

### Product Data:

#### Submit manufacturer’s printed product data literature, specifications and datasheet and include product characteristics, performance criteria, physical size, finish and limitations.

#### Submit two copies of WHMIS SDS –Safety Data Sheets.

### Test Reports

#### Submit certified test reports, from approved independent testing laboratories verifying qualities of insulation meet or exceed requirements of this specification.

#### Submit test reports in accordance with CAN/ULC-S101 for fire endurance and CAN/ULC-S102 for surface burning characteristics.

#### Submit manufacturer’s installation instructions and special handling criteria, installation sequence and cleaning procedures.

## QUALITY ASSURANCE

### Installer to conform to CUFCA Quality Assurance Program or an equivalent recognized quality assurance and training program.

### Qualifications:

#### Installer: person specializing in sprayed insulation installations with minimum 5 years experience approved by manufacturer.

#### Manufacturer: company with minimum 5 years experience in producing of material used for work required for this project, with sufficient production capacity to produce and deliver required units without causing delay in work.

## MOCK-UP

### Construct mock-up in accordance with Section 01 43 39 – Mock Up Requirements.

### Construct mock-up 10 m2 minimum, of spray in place urethane foam insulation including one inside corner and one outside corner. Mock-up may be part of finished work.

## SAFETY REQUIREMENTS

### Protect workers as recommended by CAN/ULC-S705.2 and manufacturer's recommendations:

#### Workers must wear gloves, respirators, dust masks, eye protection, protective clothing when applying foam insulation.

#### Workers must not eat, drink or smoke while applying foam insulation.

## PROTECTION

### Ventilate area in accordance with Section 01 51 00 - Temporary Utilities.

### Ventilate area to receive insulation by introducing fresh air and exhausting air continuously during and 24 hours after application to maintain non-toxic, unpolluted, safe working conditions.

### Provide temporary enclosures to prevent spray and noxious vapours from contaminating air beyond application area.

### Protect adjacent surfaces and equipment from damage by overspray, fall-out, and dusting of insulation materials.

### Dispose of waste foam daily in location designated by Owner and decontaminate empty drums in accordance with foam manufacturer’s instructions.

## ENVIRONMENTAL REQUIREMENTS

### Apply insulation only when surfaces and ambient temperatures are within manufacturers' prescribed limits.

## WARRANTY

### Provide a written guarantee, signed and issued in the name of the owner, stating the sprayed polyurethane foam insulation shall remain free from defects in materials and workmanship for a period of one (1) year from the date of Substantial Completion.

# PRODUCTS

## MATERIALS

### Insulation: spray polyurethane foam to CAN/ULC-S705.1, thickness and RSI Value as indicated on drawings.

#### Initial thermal resistance: minimum RSI 2.5 per 50 mm.

#### Long term thermal resistance: minimum RSI 2.0 per 50 mm.

#### Density: 28 kg/m3, to ASTM D1622.

#### Air barrier properties: to ASTM E2178.

##### @75 Pa: maximum 0.05 L/s.

#### Water Vapour Permeance, to ASTM E96:

##### 50 mm thick: maximum 60 ng/(Pa.s.m2).

#### Tensile Strength: minimum 200 kPa, to ASTM D1621.

#### Flame Spread: to CAN/ULC-S102, in accordance with the latest edition of the National Building Code.

#### Water Absorption by volume: maximum 4%, to ASTM D2842.

### Primers: in accordance with manufacturer's recommendations for surface conditions.

## EQUIPMENT

### Spray equipment: in accordance with CAN-ULC-S705.2 and the equipment manufacturer’s recommendations for specific type of application.

### Provide a separate proportioner unit for each spray gun.

# EXECUTION

## MANUFACTURER'S INSTRUCTIONS

### Comply with manufacturer's written recommendations or specifications, including product technical bulletins, handling, storage and installation instructions, and datasheets.

## PROTECTION OF IN-PLACE CONDITIONS

### Mask and cover adjacent areas to protect from over spray.

### Ensure any required foam stop or back up material are in place to prevent over spray and achieve complete seal.

### Seal off existing ventilation equipment. Install temporary ducting and fans to ensure exhaust fumes. Provide for make-up air.

### Erect barriers, isolate area and post warning signs to advise non-protected personnel to avoid the spay area.

## SURFACE PREPARATION

### Clean all surfaces free of oil, grease, dust and debris. Ensure surfaces are clean, dry and properly fastened to ensure adhesion of the foam to the substrate.

### Ensure that all work by other trades that may penetrates through the insulation is in place and complete

## APPLICATION

### Apply insulation to clean surfaces in accordance with CAN/ULC-S705.2 and manufacturer's printed instructions.

### Apply primer to surfaces where recommended by manufacturer. Apply primer in accordance with manufacturer’s instructions.

### Spray apply insulation to maintain continuity of thermal protection to building elements and spaces.

### Spray apply insulation to primed surfaces in accordance with CAN-ULC-S705.2.

### Spray apply insulation to final thickness as indicated on drawings. Apply in consecutive passes to thicknesses as recommended by manufacturer. Minimum thickness: 15 mm. Maximum thickness: 50 mm.

### Spray insulation to seal perimeter of electrical boxes, pipes, ducts, frames and other objects into or passing through insulation.

### Keep insulation away from heat emitting devices such as recessed light fixtures, chimneys and furnace vents. Maintain minimum distances as recommended by manufacturer's instructions.

### Finished surface of foam insulation to be free of voids and imbedded foreign objects.

### Remove masking materials and over spray from adjacent areas immediately after foam surface has hardened. Ensure cleaning methods do not damage work performed under other sections.

### Trim, as required, any excess thickness that would interfere with the application of cladding system by other trades.

### Do not enclose insulation until it has been inspected and approved by Owner.

## TOLERANCES

### Maximum variation from indicated thickness: minus 6.0 mm, plus 10 mm but not universally high or low.

## PROTECTION

### Protect installed products and accessories from damage during construction.

### Protect the spray foam from ultraviolet in accordance with manufacturer’s requirements.

### Cover the spray foam with an appropriate thermal barrier as detailed.

## FIELD QUALITY CONTROL

### Manufacturer's Field Services:

#### Provide manufacturer's field services consisting of product use recommendations and periodic site visits for inspection of product installation in accordance with manufacturer's instructions.

## CLEANING

### On completion and verification of performance of installation, remove surplus materials, excess materials, rubbish, tools and equipment.

END OF SECTION