# GENERAL

## RELATED SECTIONS

### Section 01 33 00 – Submittal Procedures.

### Section 01 43 39 – Mock Up Requirements.

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

### Section 03 30 00 - Cast-in-Place Concrete.

### Section 06 10 53 – Miscellaneous Rough Carpentry.

## REFERENCES

### Canadian General Standards Board (CGSB)

#### CAN/CGSB-51.34, Vapour Barrier, Polyethylene Sheet, for Use in Building Construction.

### Underwriters Laboratories Canada (ULC)

#### CAN/ULC S102, Method of Test for Surface Burning Characteristics of Building Materials and Assemblies.

## SUBMITTALS

### Submit manufacturer's printed product literature, specifications and datasheet and include:

#### Product characteristics.

#### Performance criteria.

#### Limitations.

### Submit two copies of Workplace Hazardous Materials Information System (WHMIS) Safety Data Sheets (SDS).

### Quality assurance submittals:

#### Certificates: submit certificates certifying that materials comply with specified performance characteristics and physical properties.

#### Instructions: submit manufacturer's installation instructions and comply with written recommendations or specifications, including product technical bulletins, handling, storage and installation instructions, and datasheet.

## MOCK-UPS

### Provide a mock-up in accordance with requirements of Section 01 43 39 – Mock Up Requirements.

### Construct mock-up of sheet vapour barrier installation including one lap joint, one inside corner and at one electrical box. Mock-up may be part of finished work.

### Mock-up will be used to judge workmanship, substrate preparation, and material application.

# PRODUCTS

## SHEET VAPOUR RETARDER

### Polyethylene film: to CAN/CGSB-51.34, 0.15mm thick with a water vapour permeance of not greater than 45 ng/(P·s·m2), flame spread rating of less than 150 to CAN/ULC S102.

## ACCESSORIES

### Joint sealing tape: air resistant pressure sensitive adhesive tape, type recommended by vapour barrier manufacturer, 50 mm wide for lap joints and perimeter seals, 25 mm wide elsewhere.

### Sealant: compatible with vapour retarder, recommended by vapour retarder manufacturer, to Section 07 92 00 - Joint Sealants.

### Staples: minimum 6 mm leg.

### Moulded box vapour barrier: factory-moulded polyethylene box for use with recessed electric switch and outlet device boxes.

# EXECUTION

## INSTALLATION

### Ensure services are installed and inspected prior to installation of retarder.

### Install sheet vapour retarder on warm side of exterior wall and ceiling space assemblies prior to installation of gypsum board to form continuous retarder.

### Install Sheet Vapour retarder under stone cover in crawl space to form continuous retarder.

### Use sheets of largest practical size to minimize joints.

### Inspect for continuity. Repair punctures and tears with sealing tape before work is concealed.

## EXTERIOR SURFACE OPENINGS

### Cut sheet vapour retarder to form openings and ensure material is lapped and sealed to frame.

## PERIMETER SEALS

### Seal perimeter of sheet vapour barrier as follows:

#### Apply continuous bead of sealant to substrate at perimeter of sheets.

#### Lap sheet over sealant and press into sealant bead.

#### Install staples through lapped sheets at sealant bead into wood substrate.

#### Ensure that no gaps exist in sealant bead. Smooth out folds and ripples occurring in sheet over sealant.

## LAP JOINT SEALS

### Seal lap joints of sheet vapour barrier as follows:

#### Attach first sheet to substrate.

#### Apply continuous bead of sealant over solid backing at joint.

#### Lap adjoining sheet minimum 150 mm and press into sealant bead.

#### Install staples through lapped sheets at sealant bead into wood substrate.

#### Ensure that no gaps exist in sealant bead. Smooth out folds and ripples occurring in sheet over sealant.

## ELECTRICAL BOXES

### Seal electrical switch and outlet device boxes that penetrate vapour barrier as follows:

#### Install moulded box vapour barrier or wrap boxes with film sheet providing minimum 300 mm perimeter lap flange.

#### Apply sealant to seal edges of flange to main vapour barrier and seal wiring penetrations through box cover.

## CLEANING

### Upon completion and verification of performance of installation, remove surplus materials, excess materials, rubbish, tools and equipment.

END OF SECTION