# GENERAL

## SECTION INCLUDES

### Materials, removal and installation of fiberglass-reinforced asphalt shingles and roll roofing.

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 01 45 00 - Quality Control.

### Section 01 61 00 - Common Product Requirements.

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

### Section 01 78 00 - Closeout Submittals.

### Section 07 62 00 – Sheet Metal Flashing and Trim.

## REFERENCES

### Canadian General Standards Board (CGSB).

#### CAN/CGSB-37.4, Fibrated, Cutback Asphalt, Lap Cement for Asphalt Roofing.

#### CAN/CGSB-37.5, Cutback Asphalt Plastic Cement.

#### CAN/CGSB-51.32, Sheathing, Membrane, Breather Type.

#### CAN/CGSB-51.34, Vapour Barrier Polyethylene Sheet, for Use in Building Construction.

### Canadian Roofing Contractors' Association (CRCA).

#### CRCA Roofing Specification Manual.

### Canadian Standards Association (CSA).

#### CAN/CSA-A123.1/A123.5, Asphalt Shingles Made From Organic Felt and Surfaced With Mineral Granules/Asphalt Shingles Made From Glass Felt and Surfaced With Mineral Granules.

#### CSA A123.2, Asphalt-Coated Roofing Sheets.

#### CAN/CSA-A123.3, Asphalt Saturated Organic Roofing Felt.

#### CAN3-A123.51, Asphalt Shingle Application on Roof Slopes 1:3 and Steeper.

#### CAN3-A123.52, Asphalt Shingle Application on Roof Slopes 1:6 to Less Than 1:3.

#### CSA B111, Wire Nails, Spikes and Staples.

### National Research Council Canada (NRC)/Institute for Research in Construction (IRC) - Canadian Construction Materials Centre (CCMC).

#### CCMC, Registry of Product Evaluations.

## SUBMITTALS

### Manufacturer's Instructions: Provide to indicate special handling criteria, installation sequence, cleaning procedures.

### Submit product data sheets for asphalt shingles. Include:

#### Product characteristics.

#### Performance criteria.

#### Installation instructions.

#### Limitations.

#### Colour and finish.

### Submit duplicate samples of full size specified shingles.

## DELIVERY, STORAGE AND HANDLING

### Deliver, handle, store and protect materials in accordance with Section 01 61 00 - Common Product Requirements.

### Provide and maintain dry, off-ground weatherproof storage.

### Remove only in quantities required for same day use.

## WASTE MANAGEMENT AND DISPOSAL

### Place materials defined as hazardous or toxic in designated containers.

### Ensure emptied containers are sealed and stored safely for disposal away from children.

### Use the least toxic sealants, and adhesives necessary to comply with requirements of this section.

### Close and seal tightly. Remove from site and dispose of all packaging materials at appropriate recycling facilities.

### Place used hazardous sealant tubes and adhesive containers in areas designated for hazardous materials.

## WARRANTY

### Provide a written guarantee, signed and issued in the name of the owner, stating the fiberglass-reinforced asphalt shingles shall remain free from defects in materials and workmanship for a period of twenty five (25) years from the date of Substantial Completion.

# PRODUCTS

## MATERIALS

### Fiberglass-reinforced asphalt shingles: to CSA A123.1/A123.5.

#### Type: self-seal, standard, pattern rectangular.

#### Mass: minimum 33 kg/3m².

#### Colours:  as selected by Owner.

### Roofing underlayment: self-adhesive, non-woven glass fibre matt coated with SBS modified bitumen, minimum thickness 1.8 mm, bottom surface release film, top surface sanded.

### Continuous Ridge Vent: minimum 285 mm wide durable, copolymer plastic ridge vent, providing minimum 357 cm2/m net free vent area, capable of accepting fiberglass-reinforced asphalt shingle cap over for shingle finish.

### PVC drip edge: extruded profile of unplasticized polyvinyl chloride of minimum thickness of 0.8 mm.

### Cement: Plastic cement: to CAN/CGSB-37.5.

### Nails: to CSA B111, of galvanized steel, sufficient length to penetrate 19 mm into deck.

# EXECUTION

## REMOVAL OF EXISTING ROOFING

### Remove existing roofing, flashings and underlay, and expose sheathing or shingle lath of roof.

### Withdraw existing shingle and flashing nails, set those which break off. Leave surfaces free from dirt and loose material.

### Owner to inspect roof sheathing. Take up, cut out, portion of sheathing boards affected by fungal or insect attack as directed on site by Owner.

### Replace cut out portions of sheathing or lath with sheathing of equal sectional dimensions, and specified grade. Seat each end of board on rafter/truss, with 25mm bearing, and secure to rafter/truss.

## APPLICATION

### Do fiberglass-reinforced asphalt shingle work in accordance with CAN3-A123.51/CAN3-A123.52, NBC/CRCA Specification, except where specified otherwise.

### Install layer of self-adhesive roof underlayment over the entire roof area.

### Install drip edge along eaves, overhanging 12 mm, with minimum 50 mm flange extending onto roof decking. Nail to deck at 400 mm oc.

### Install bottom step flashing (soaker base flashing) interleafed between shingles at vertical junctions.

### Install fiberglass-reinforced asphalt shingles on roof slopes 1:3 and steeper in accordance with CAN3-A123.51 supplemented as follows:

### Install fiberglass-reinforced asphalt shingles on roof slopes 1:6 to less than 1:3 in accordance with CAN3-A123.52 supplemented as follows.

## PROTECTION

### Protect installed products and components from damage during construction.

### Repair damage to adjacent materials caused by asphalt shingles installation.

END OF SECTION