# GENERAL

## RELATED SECTIONS

### Section 01 33 00 – Submittal Procedures.

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

### Section 06 10 53 – Miscellaneous Rough Carpentry.

### Section 07 62 00 – Sheet Metal Flashing and Trim.

### Section 07 92 00 - Joint Sealants.

## REFERENCES

### American Society of Mechanical Engineers (ASME)

#### ASME B18.6.3, Machine Screws, Tapping Screws, and Metallic Drive Screws (Inch Series).

### ASTM International

#### ASTM B209, Standard Specification for Aluminum and Aluminum-Alloy Sheet and Plate.

#### ASTM D2369, Test Method for Volatile Content of Coatings.

#### ASTM D2832, Standard Guide for Determining Volatile and Nonvolatile Content of Paint and Related Coatings.

#### ASTM D5116, Standard Guide For Small-Scale Environmental Chamber Determinations of Organic Emissions From Indoor Materials/Products.

### Canadian General Standards Board (CGSB)

#### CAN/CGSB-51.32, Sheathing, Membrane, Breather Type.

#### CAN/CGSB-93.2, Prefinished Aluminum Siding, Soffits and Fascia, for Residential Use.

#### CAN/CGSB-93.3, Prefinished Galvanized and Aluminum-Zinc Alloy Steel Sheet for Residential Use.

#### CAN/CGSB-93.4, Galvanized and Aluminum-Zinc Alloy Coated Steel Siding Soffits and Fascia, Prefinished, Residential.

#### CGSB 93.5, Installation of Metal Residential Siding, Soffits and Fascia.

### Canadian Standards Association (CSA)

#### CSA B111, Wire Nails, Spikes and Staples.

## SUBMITTALS

### Product data: submit manufacturer's printed product literature, specifications and data sheet.

#### Submit two copies of WHMIS SDS - Safety Data. Indicate VOC's for caulking materials during application and curing.

### Submit duplicate 300 x 300 mm samples of siding material, of colour and profile specified.

### Shop drawings to indicate dimensions, profiles, attachment methods, schedule of wall elevations, trim and closure pieces, soffits, fascia, metal furring, and related work.

### Submit manufacturer’s installation instructions.

## Warranty

### Provide a written guarantee, signed and issued in the name of the owner, covering the metal cladding/siding material for 10 (ten) years and workmanship for a period of 2 (years) years from the date of Substantial Completion.

### Areas which prove to be defective in any way shall be repaired or replaced and any damage to other work as a result of such defects shall be repaired at no cost to the Owner.

# PRODUCTS

## ALUMINUM CLADDING AND COMPONENTS

### Strip siding: to ASTM B209, Type A vertical, Class 1.

#### Finish coating: silicone modified polyester (SMP) topcoat system.

#### Colour: colour selected by Owner.

#### Gloss: 30 ± 5.

#### Thickness: 0.65 mm base metal thickness.

#### Profile: preformed interlocking joints, fastener holes prepunched, profile as indicated on drawings.

### Soffit: to ASTM B209, Type B, Class 1

#### Finish coating: silicone modified polyester (SMP) topcoat system.

#### Colour: selected by Owner.

#### Gloss: 30 ± 5.

#### Thickness: 0.65 mm base metal thickness.

#### Profile:  flat sheet “V” crimped for stiffness, vented 0.1m2 of opening for every 30 m 2 of building area.

### Fascia facings and exposed trim: to ASTM B209, Type C, Class 1

#### Finish coating: silicone modified polyester (SMP) topcoat system.

#### Colour: colour selected by Owner.

#### Gloss: 30 ± 5.

#### Thickness: 0.65 mm base metal thickness.

#### Profile: flat sheet ”V” crimped for stiffness, preformed with elongated slits and small perforations.

## ACCESSORIES

### Exposed trim: inside corners, outside corners, cap strip, drip cap, undersill trim, starter strip and window/door trim of same material, colour and gloss as cladding, with fastener holes pre-punched.

## FASTENERS

### Nails: to CSA B111. Screws to ASME B18.6.3. Purpose made aluminum alloy stainless steel.

## CAULKING

### Sealants: Section 07 92 00 – Joint Sealants.

## SHEATHING membrane

### Exterior wall sheathing membrane: to CAN2-51.32, single ply spunbound olefin type coated.

# EXECUTION

## INSTALLATION

### Install cladding in accordance with CGSB 93.5, and manufacturer's written instructions

### Install one layer exterior wall sheathing membrane horizontally by stapling or nailing lapping edges 150 mm.

### Install continuous starter strips, inside and outside corners, edgings, soffit, drip, cap, sill and window/door opening flashings as indicated.

### Install outside corners, fillers and closure strips with carefully formed and profiled work.

### Install soffit and fascia cladding as indicated.

### Maintain joints in exterior cladding, true to line, tight fitting, hairline joints.

### Attach components in manner not restricting thermal movement.

### Caulk junctions with adjoining work with sealant. Do work in accordance with Section 07 92 00 - Joint Sealants.

## CLEANING

### Upon completion of installation, remove surplus materials, rubbish, tools and equipment barriers.

## PROTECTION

### Protect installed products and components from damage during construction.

### Repair damage to adjacent materials caused by preformed metal siding installation.

END OF SECTION