# GENERAL

## RELATED SECTIONS

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

### Section 06 10 53 – Miscellaneous Rough Carpentry.

### Section 07 62 00 – Sheet Metal Flashing and Trim.

### Section 07 92 00 - Joint Sealants.

## REFERENCES

### American National Standards Institute (ANSI)

#### ANSI A135.6, Hardboard Siding Standard.

### Canadian General Standards Board (CGSB)

#### CAN/CGSB-11.3, Hardboard.

#### CAN/CGSB-11.5, Hardboard, Precoated, Factory Finished, for Exterior Cladding.

#### CAN/CGSB-11.6, Installation of Exterior Hardboard Cladding.

#### CAN/CGSB-51.32, Sheathing, Membrane, Breather Type.

### Canadian Standards Association (CSA)

#### CSA B111, Wire Nails, Spikes and Staples.

#### CSA O121, Douglas Fir Plywood.

#### CSA O151, Canadian Softwood Plywood.

### National Lumber Grading Authority (NLGA)

#### NLGA Standard Grading Rules for Canadian Lumber.

## SUBMITTALS

### Product Data:

#### Submit manufacturer's printed product literature, specifications and data sheet.

#### Submit copies of WHMIS SDS - Safety Data Sheets. Indicate VOC's for caulking materials during application and curing.

### Submit duplicate 300 x 300 mm size profile specified.

### Submit manufacturer’s installation instructions.

## DELIVERY, STORAGE AND HANDLING

### Deliver, handle, store and protect materials in accordance with Section 01 61 00 – Common Product Requirements.

### Deliver siding suitable packaged to avoid damage to finished surface.

### Store in an unheated structure or under cover until application. Siding may be temporarily stored outside if at least 100 mm off the ground and on a flat, well drained surface protected from moisture with a shed pack or waterproof cover.

## QUALITY ASSURANCE

### Provide Certificate of Quality Compliance from siding manufacturer upon completion of fabrication.

### Provide Certificate of Quality Compliance upon satisfactory completion of installation.

## WARRANTY

### Warranty Period: 15 years against cracking, peeling, blistering, chalking, loss of coating adhesion, yellowing with age, and no damage caused by rinse cleaning surface dirt.  Warranty to commence at date of Substantial Completion.

# PRODUCTS

## MATERIALS

### Clapboard Siding: Western Lodgepole Pine or Eastern Spruce, NO. 1 select or better grade, factory finished, saw texture, bevel profile, cove or V-joint pattern, free of large knots, knot holes, or loose knots: maximum moisture content of 12 percent. Size: 16 mm thickness, 150 mm width, 114 mm actual coverage.

### Moldings and trim: Western Lodgepole Pine or Eastern Spruce, No. 1 select or better grade, factory finished same as siding.

### Strapping: Softwood Lumber, kiln dried treated with brush applied wood preservative.

### Nails: Mechanically galvanized, to securely and rigidly retain the work permanently in position, pre-finished baked on coating to match siding finish. Nails 64 mm long for siding and 83 mm for trims.

### Exterior Sheathing Membrane:  CAN/CGSB 51.32M, Spun bonded olefin sheeting, conforming to ASTM D3575, single ply laminated and coated.

### Sealant: Thermoplastic type, color to exactly match siding.

### Concealed Flashings: 0.4 mm thick galvanized steel.

## FINISH

### Pre-finish color: Thermoplastic acrylic latex emulsion, factory coated under controlled environment conditions by a modified vacuum coat method, one prime coat and one finish coat, applied to all board surfaces, minimum 0.15 mm dry film thickness.

#### Standard color or custom color from manufacturers range of colors.

#### Touch-Up Paint: Thermoplastic acrylic latex emulsion, same type and color as siding.

# EXECUTION

## EXAMINATION

### Verify that substrate surfaces and wall openings are ready to receive work.

## PREPARATION

### Install metal flashing continuous over window and other openings. Secure in position tight to wall sheathing.

### Install one layer of sheathing membrane horizontally on sheathed walls, weather lap edges and ends minimum 150 mm. Stagger vertical laps.  Tape all edges.

### Install strapping at 460 mm o.c.

### Install siding kitchen starter strips, behind first row of siding.

### Apply sealant around window, door and other opening frames.

## INSTALLATION

### Install siding and accessories to manufacturer’s instructions.

### Install screen at bottom of base trim.

### Install siding for natural watershed.

### Install sill flashings, wood starter strips, inside corner flashings, edgings and flashings over openings.

### Install hardboard to CGSB11-GP-6M and manufacturers' instructions.

### Achieve siding joints no less that 800 mm apart in adjoining boards and distribute evenly over wall surface.

### Miter external and internal corners: Install corner strips, closures, frieze boards skirt boards and trim.

### Fasten siding securely to wood batten substrate.

### Face nail 25 mm from bottom of siding board directly into wood strapping, drive nail head just flush with siding surface; do not indent or penetrate painted coating.

## INCIDENTAL SITE FINISHING

### Carefully set exposed nails flush with siding coating.

### Touch-up blemished siding materials to match siding color.

## CLEANING

### Upon completion of installation, remove surplus materials, rubbish, tools and equipment barriers.

## PROTECTION

### Protect installed products and components from damage during construction.

### Repair damage to adjacent materials caused by preformed metal siding installation.

END OF SECTION