# General

## SECTION INCLUDES

### Moisture testing of substrates.

### Surface preparation of substrates as required for acceptance of paint, including cleaning, small crack repair, patching, caulking, and making good surfaces and areas to limits defined under MPI Repainting Maintenance Manual requirements.

### Specific pre-treatments noted herein or specified in the MPI Repainting Maintenance Manual.

### Sealing/touch-up, spot priming, and/or full priming surfaces for repainting in accordance with MPI Repainting Maintenance Manual requirements.

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 01 43 39 – Mock Up Requirements.

### Section 01 45 00 - Quality Control.

### Section 01 61 00 - Common Product Requirements.

### Section 01 74 21 - Construction/Demolition Waste Management and Disposal.

### Section 01 78 00 - Closeout Submittals.

### Section 09 01 90.63 - Interior Re-Painting.

### Section 09 91 13 - Exterior Painting.

### Section 09 91 23 - Interior Painting.

## REFERENCES

### Maintenance Repainting Manual by the Master Painters Institute (MPI), including Identifiers, Evaluation, Systems, Preparation and Approved Product List.

### Test Method for Measuring Total Volatile Organic Compound Content of Consumer Products, Method 24 (for Surface Coatings) of the Environmental Protection Agency (EPA).

### National Fire Code of Canada.

## QUALITY ASSURANCE

### Contractor shall have a minimum of five years proven satisfactory experience.  Provide a list of last three comparable jobs including, job name and location, specifying authority, and project manager.

### Qualified journeymen who have a "Tradesman Qualification Certificate of Proficiency" shall be engaged in painting work. Apprentices may be employed provided they work under the direct supervision of a qualified journeyman in accordance with applicable trade regulations.

### Conform to latest MPI requirements for exterior repainting work including cleaning, preparation and priming.

### Materials (primers, paints, coatings, varnishes, stains, lacquers, fillers, thinners, solvents, etc.) shall be in accordance with the latest edition of the MPI Approved Product List and shall be from a single manufacturer for each system used.

### Paint materials such as linseed oil, shellac, turpentine, etc. shall be the highest quality product of an approved manufacturer listed in MPI Maintenance Repainting Manual and shall be compatible with other coating materials as required.

### Retain purchase orders, invoices and other documents to prove conformance with noted MPI requirements when requested by Owner.

### Standard of Acceptance: When viewed using natural prevailing sunlight at peak period of the day (mid-day) on surface viewed, surfaces shall indicate the following:

#### Walls:  No defects visible from a distance of 1000 mm at 90o to surface.

#### Soffits:  No defects visible from grade at 45o to surface.

#### Final coat to exhibit uniformity of colour and sheen across full surface area.

## ENVIRONMENTAL PERFORMANCE REQUIREMENTS

### Provide paint products meeting MPI "Environmentally Friendly" E2 or E3 ratings based on VOC (EPA Method 24) content levels.

## SCHEDULING OF WORK

### Submit work schedule for various stages of painting to Owner for approval. Submit schedule a minimum of two (2) working days in advance of proposed operations.

### Paint occupied facilities in accordance with approved schedule. Schedule operations to approval of Owner such that painted surfaces will have dried and cured sufficiently before occupants are affected.

### Obtain written authorization from Owner for changes in work schedule.

### Schedule repainting operations to prevent disruption by other trades if applicable and by occupants in and about the building.

## SUBMITTALS

### Submit full range colour sample chips for review and selection.  Indicate where colour availability is restricted.

### Submit product data and manufacturer's installation/application instructions for paints and coating products to be used.

### Submit WHMIS Safety Data Sheets (SDS) for paints and coating materials to be used.

### Upon completion, submit records of products used.  List products in relation to finish system and include the following:

#### Product name, type and use (i.e. materials and location).

#### Manufacturer's product number.

#### Colour code numbers.

#### MPI Environmentally Friendly classification system rating.

#### Manufacturer's Safety Data Sheets.

### Submit duplicate 200 x 300 mm sample panels of each paint, stain, clear coating, with specified paint or coating in colours, gloss/sheen and textures required to MPI Painting Specification Manual standards submitted on the following substrate materials:

#### 3.0 mm plate steel for finishes over metal surfaces.

#### 13 mm birch plywood for finishes over wood surfaces.

#### 50 mm concrete block for finishes over concrete or concrete masonry surfaces.

#### 13 mm gypsum board for finishes over gypsum board and other smooth surfaces.

### When approved, samples shall become acceptable standard of quality for appropriate on-site surface with one of each sample retained on-site.

## QUALITY CONTROL

### Provide a mock-up in accordance with requirements of Section 01 43 39 – Mock Up Requirements.

### Prepare and repaint mock-up designated exterior surface or item to requirements specified herein, with specified paint or coating showing selected colours, gloss/sheen, textures and workmanship to MPI Maintenance Repainting Manual standards for review and approval.

## DELIVERY, HANDLING AND STORAGE

### Deliver, store and handle materials in accordance with Section 01 61 00 - Common Product Requirements.

### Deliver and store materials in original containers, sealed, with labels intact.

### Labels shall clearly indicate:

#### Manufacturer's name and address.

#### Type of paint or coating.

#### Compliance with applicable standard.

#### Colour number in accordance with established colour schedule.

### Remove damaged, opened and rejected materials from site.

### Observe manufacturer's recommendations for storage and handling.

### Store materials and equipment in a secure, dry, well-ventilated area with temperature range between 7o C to 30o C. Store materials and supplies away from heat generating devices and sensitive products above minimum temperature as recommended by manufacturer.

### Keep areas used for storage, cleaning and preparation, clean and orderly to approval of Owner. Upon completion of operations, return areas to clean condition to approval of Owner.

### Remove paint materials from storage in quantities required for same day use.

### Comply with requirements of Workplace Hazardous Materials Information System (WHMIS) regarding use, handling storage, and disposal of hazardous materials.

### Fire Safety Requirements:

#### Provide one 9 kg Type ABC dry chemical fire extinguisher adjacent to storage area.

#### Store oily rags, waste products, empty containers and materials subject to spontaneous combustion in ULC approved, sealed containers and remove from site on a daily basis.

#### Handle, store, use and dispose of flammable and combustible materials in accordance with the National Fire Code of Canada.

## SITE REQUIREMENTS

### Heating, Ventilation and Lighting:

#### Ventilate enclosed spaces.

#### Perform no painting work unless adequate and continuous ventilation and sufficient heating facilities are in place to maintain ambient air and substrate temperatures above 10º C for 24 hours before, during and after paint application until paint has cured sufficiently.

#### Where required, provide continuous ventilation for seven days after completion of application of paint.

#### Provide temporary ventilating and heating equipment where permanent facilities are not available.

#### Perform no painting work unless a minimum lighting level of 323 Lux is provided on surfaces to be painted.  Adequate lighting facilities shall be provided by General Contractor.

### Temperature, Humidity and Substrate Moisture Content Levels:

#### Unless specifically pre-approved by Owner and applied product manufacturer, do not perform repainting work when:

##### Ambient air and substrate temperatures are below 10o C.

##### Substrate temperature is over 32o C unless paint is specifically formulated for application at high temperatures.

##### Substrate and ambient air temperatures are expected to fall outside MPI or paint manufacturer's prescribed limits.

##### Relative humidity is above 85% or when dew point is less than 3o C variance between air/surface temperature.

##### Rain or snow is forecast to occur before paint has thoroughly cured.

##### It is foggy, misty, raining or snowing at site.

#### Conduct moisture tests using a properly calibrated electronic Moisture Meter, except test existing painted concrete floors for moisture using a simple "cover patch test".

#### Do not perform repainting work when maximum moisture content of substrate exceeds:

##### 12% for concrete and masonry (clay and concrete brick/block).

##### 15% for wood.

##### 12% for stucco.

#### Test painted concrete, masonry and plaster surfaces for alkalinity as required.

### Application Requirements:

#### Apply paint finish in areas where dust is no longer being generated by related construction operations or when wind conditions are such that airborne particles will affect quality of finished surface.

#### Apply paint to adequately prepared surfaces and to surfaces within moisture limits noted herein.

#### Apply paint when previous coat of paint is dry or adequately cured, unless otherwise pre-approved by specific coating manufacturer.

#### Apply paint finishes when conditions forecast for entire period of application fall within manufacturer's recommendations.

#### Do not apply paint when:

##### Temperature is expected to drop below 10o C before paint has thoroughly cured.

##### Substrate and ambient air temperatures are expected to fall outside MPI or paint manufacturer's limits.

##### Surface to be painted is wet, damp or frosted.

#### Provide and maintain cover when paint must be applied in damp or cold weather. Heat substrates and surrounding air to comply with temperature and humidity conditions specified by manufacturer. Protect until paint is dry or until weather conditions are suitable.

#### Schedule repainting operations such that surfaces exposed to direct, intense sunlight are scheduled for completion during early morning.

#### Remove paint from areas which have been exposed to freezing, excess humidity, rain, snow or condensation. Prepare surface again and repaint.

## WASTE MANAGEMENT AND DISPOSAL

### Separate and recycle waste materials in accordance with Section 01 74 21 - Construction/Demolition Waste Management and Disposal.

### Remove from site and dispose of packaging materials at appropriate recycling facilities.

### Place materials defined as hazardous or toxic in designated containers.

### Ensure emptied containers are sealed and stored safely.

### Unused paint, coating materials must be disposed of at official hazardous material collections site as approved by Owner.

### Paint, stain and wood preservative finishes and related materials (thinners, solvents, etc.) are hazardous products and are subject to regulations for disposal.  Information on these controls can be obtained from Provincial Ministries of Environment and Regional levels of Government.

### Materials that cannot be reused must be treated as hazardous waste and disposed of in an appropriate manner.

### Place materials defined as hazardous or toxic waste, including used sealant and adhesive tubes and containers, in containers or areas designated for hazardous waste.

### To reduce the amount of contaminants entering waterways, sanitary/storm drain systems or into the ground the following procedures shall be strictly adhered to:

#### Retain cleaning water for water-based materials to allow sediments to be filtered out.  In no case shall equipment be cleaned using free draining water.

#### Retain cleaners, thinners, solvents and excess paint and place in designated containers and ensure proper disposal.

#### Return solvent and oil soaked rags used during painting operations for contaminant recovery, proper disposal, or appropriate cleaning and laundering.

#### Dispose of contaminants in an approved legal manner in accordance with hazardous waste regulations.

### Empty paint cans are to be dry prior to disposal or recycling (where available).

### Close and seal tightly partly used cans of materials including sealant and adhesive containers and store protected in well ventilated fire-safe area at moderate temperature.

# Products

## MATERIALS

### Paint materials listed in the latest edition of the MPI Approved Product List (APL) are acceptable for use on this project.

### Paint materials for repaint systems shall be products of a single manufacturer.

### Low odour products: whenever possible, select products exhibiting low odour characteristics. If two products are otherwise equivalent, select the product with the lowest odour. Only qualified products with E2 or E3 "Environmentally Friendly" rating are acceptable for use on this project.

### Paints, coatings, thinners, solvents, cleaners and other fluids used in repainting, shall:

#### Be water-based, water soluble, water clean-up.

#### Be non-flammable

#### Not contain methylene chloride, chlorinated hydrocarbons, toxic metal pigments.

#### Be manufactured without compounds which contribute to ozone depletion in the upper atmosphere.

#### Be manufactured without compounds which contribute to smog in the lower atmosphere.

### Paints and coatings must be manufactured and transported in a manner that steps of processes, including disposal of waste products arising therefrom, will meet requirements of applicable governmental acts, by-laws and regulations including, for facilities located in Canada, Fisheries Act and Canadian Environmental Protection Act (CEPA).

### Paints and coatings must not be formulated or manufactured with formaldehyde, halogenated solvents, mercury, lead, cadmium, hexavelant chromium or their compounds.

### Both water-borne surface coatings and recycled water-borne surface coatings must be made by a process that does not release:

#### Matter in undiluted production plant effluent generating a 'Biochemical Oxygen Demand' (BOD) in excess of 15 mg/L to a natural watercourse or a sewage treatment facility lacking secondary treatment.

#### Total Suspended Solids (TSS) in undiluted production plant effluent in excess of 15 mg/L to a natural watercourse or a sewage treatment facility lacking secondary treatment.

### Water-borne paints and stains, and water borne varnishes must meet a minimum "Environmentally Friendly" E2 rating.

## COLOURS

### Owner will provide Colour Schedule after Contract award.

### Selection of colours will be from manufacturer’s full range of colours.

### Where specific products are available in a restricted range of colours, selection will be based on the limited range.

### Second coat in a three coat repaint system to be tinted slightly lighter colour than top coat to show visible difference between coats.

## MIXING AND TINTING

### Perform colour tinting operations prior to delivery of paint to site. On-site tinting of painting materials is allowed with Ownerwritten permission.

### Paste, powder or catalyzed paint mixes shall be mixed in strict accordance with manufacturer's written instructions.

### Where thinner is used, addition shall not exceed paint manufacturer's recommendations.  Do not use kerosene or such organic solvents to thin water-based paints.

### Thin paint for spraying according in strict accordance with paint manufacturer's instructions.  If directions are not on container, obtain instructions in writing from manufacturer and provide copy of instructions to Owner.

### Re-mix paint in containers prior to and during application to ensure break-up of lumps, complete dispersion of settled pigment, and colour and gloss uniformity.

## GLOSS / SHEEN RATINGS

### Paint gloss shall be defined as the sheen rating of applied paint, in accordance with the following MPI gloss/sheen standard values:

| Gloss Level Category | Units @ 60o | Units @ 85o |
| --- | --- | --- |
| G1 - matte finish | 0 to 5 | maximum 10 |
| G2 - velvet finish | 0 to 10 | 10 to 35 |
| G3 - eggshell finish | 10 to 25 | 10 to 35 |
| G4 - satin finish | 20 to 35 | minimum 35 |
| G5 - semi-gloss finish | 35 to 70 |  |
| G6 - gloss finish | 70 to 85 |  |
| G7 - high gloss finish | > 85 |  |

### Gloss level ratings of repainted surfaces shall be as specified herein.

## EXTERIOR PAINTING SYSTEMS

### The following paint formulas requires a two coat finish as indicated in the MPI Repainting Maintenance Manual.

### REX 2.1 - Asphalt Surfaces: Zone/Traffic Marking for Drive and Parking Areas, etc.

#### REX 2.1B - Alkyd Zone/Traffic Marking Finish.

### REX 3.1 - Concrete Vertical Surfaces:  (including horizontal soffits).

#### REX 3.1A - Latex G4 finish.

### REX 3.2 - Concrete Horizontal Surfaces:  (decks, stairs, parking and court areas, driveways, etc.).

#### REX 3.2A - Latex Floor Paint G4.

### REX 4.1 - Clay Masonry Units:  (Pressed and Extruded Brick).

#### REX 4.1A - Latex G4 finish.

### REX 4.2 - Concrete Masonry Units: (Concrete Block and Brick).

#### REX 4.2A - Latex G4 finish.

### REX 5.1 - Structural Steel and Metal Fabrications:  (columns, beams, joists, etc.).

#### REX 5.1F - 2 Component Epoxy finish.

### REX 5.3 - Galvanized Metal: High Contact/High Traffic Areas (Doors, Frames, Railings, Pipes, Handrail, etc. Low Contact/Low Traffic Areas (Overhead Decking, Eavestrough (Gutters), Downpipes, Ducts, etc.

#### REX 5.3B - Alkyd G5 finish.

### REX 6.2 - Dimension Lumber:  (columns, beams, exposed joists, underside of decking, siding, fencing, etc.).

#### REX 6.2A - Latex G4 (over latex primer).

#### REX 6.2E - Semi-Transparent Stain.

### REX 6.3 - Dressed Lumber:  (doors, door and window frames, casings, battens, smooth fascias, etc.)

#### REX 6.3L - Latex G4 finish.

### REX 6.4 - Wood Panelling: (plywood siding, fascias, soffits, etc.).

#### REX 6.4G - Latex G4 finish.

### REX 6.5 - Wood Decks and Stairs/Steps:  (using spaced lumber).

#### REX 6.5A - Porch and Floor Acrylic Latex G4 finish (over primer).

#### REX 6.5C - Deck Stain.

# Execution

## GENERAL

### Perform preparation and operations for exterior painting in accordance with MPI Maintenance Repainting requirements except where specified otherwise.

### Apply paint materials in accordance with paint manufacturer's written application instructions.

## EXISTING CONDITIONS

### Prior to commencing work, thoroughly examine site conditions and existing exterior substrates to be repainted and report in writing to Owner damages, defects, unsatisfactory or unfavourable conditions of surfaces that will adversely affect this work.

### Conduct moisture testing of surfaces to be painted using a properly calibrated electronic moisture meter, except test concrete floors for moisture using a simple "cover patch test" and report findings to Owner. Do not proceed with work until conditions fall within acceptable range as recommended by manufacturer.

### Maximum moisture content as follows:

#### Concrete: 12%.

#### Clay and Concrete Block/Brick: 12%.

#### Wood: 15%.

### No repainting work shall commence until such adverse conditions and defects have been corrected and surfaces and conditions are acceptable to the Painting Subcontractor and Inspection Agency. Commencement of work shall not be held to imply acceptance of surfaces except as qualified herein.

### Degree of surface deterioration (DSD) shall be assessed using MPI Identifiers and Assessment criteria indicated in the MPI Maintenance Repainting Manual.  MPI DSD ratings and descriptions are as follows:

| Condition | Description |
| --- | --- |
| DSD-0 | Sound Surface ( includes visual (aesthetic) defects that do not affect film's protective properties). |
| DSD-1 | Slightly Deteriorated Surface (indicating fading; gloss reduction, slight surface contamination, minor pin holes scratches, etc.). |
| DSD-2 | Moderately Deteriorated Surface (small areas of peeling, flaking, slight cracking, staining, etc.). |
| DSD-3 | Severely Deteriorated Surface (heavy peeling, flaking, cracking, checking, scratches, scuffs, abrasion, small holes and gouges). |
| DSD-4 | Substrate Damage (repair or replacement of surface required by others). |

## PROTECTION

### Protect existing building surfaces and adjacent structures from paint spatters, markings and other damage by suitable non-staining covers or masking.  If damaged, clean and restore such surfaces as directed by Owner.

### Cover or mask windows and other ornamental hardware adjacent to areas being painted to prevent damage and to protect from paint drops and splatters. Use non-staining coverings.

### Protect items that are permanently attached such as Fire Labels on doors and frames.

### Protect factory finished products and equipment.

### Protect general public and building occupants in and about the building.

### Remove electrical cover plates, light fixtures, surface hardware on doors, and surface mounted equipment, fittings and fastenings prior to undertaking painting operations.  Items shall be securely stored and re-installed after painting is completed.

### Move and cover exterior furniture and portable equipment as necessary to carry out painting operations.  Replace as painting operations progress.

### As painting operations progress, place "WET PAINT" signs in pedestrian and vehicle traffic areas to approval of Owner.

## CLEANING AND PREPARATION

### Clean and prepare exterior surfaces to be repainted in accordance with MPI Maintenance Repainting Manual requirements.  Refer to MPI Manual in regard to specific requirements and as follows:

#### Remove dust, dirt, and surface debris by wiping with dry, clean cloths or compressed air.

#### Wash surfaces with a biodegradable detergent and bleach where applicable and clean warm water using a stiff bristle brush to remove dirt, oil and surface contaminants.

#### Rinse scrubbed surfaces with clean water until foreign matter is flushed from surface.

#### Use trigger operated spray nozzles for water hoses.

#### Allow surfaces to drain completely and to dry thoroughly.

#### Use water-based cleaners in place of organic solvents where surfaces will be repainted using water based paints.

#### Many water-based paints cannot be removed with water once dried.  However, minimize the use of kerosene or such organic solvents to clean up water-based paints.

### Where required, pressure wash exterior surfaces prior to repainting in accordance with MPI standards for type of surfaces and recommended pressures to ensure complete removal of loose paint, stains, dirt, and foreign matter.  This work to be carried out by qualified tradesman experienced in pressure water cleaning. Use of spray equipment such as water hose cleaning will not be considered satisfactory unless specified herein. Allow sufficient drying time and test surfaces using an electronic moisture meter before commencing work.

### Clean metal surfaces to be repainted by removing rust, dirt, oil, grease and foreign substances in accordance with MPI requirements.  Remove such contaminates from surfaces, pockets and corners to be repainted by brushing with clean brushes, blowing with clean dry compressed air, or brushing/vacuum cleaning as required.

### Prevent contamination of cleaned surfaces by salts, acids, alkalis, corrosive chemicals, grease, oil and solvents before priming and between applications of remaining coats.  Touch-up, spot prime, and apply primer, paint, or pre-treatment as soon as possible after cleaning and before deterioration occurs.

### Do not apply paint until prepared surfaces have been accepted by Owner.

### Sand and dust between coats as required to provide adequate adhesion for next coat and to remove defects from previously painting (e.g. runs, sags, etc.) that are visible from a distance up to 1000 mm.

## APPLICATION

### Method of application to be as approved by Owner.  Apply paint by brush, roller, air sprayer, airless sprayer.  Conform to manufacturer's application instructions unless specified otherwise.

### Brush and Roller Application:

#### Apply paint in a uniform layer using brush and/or roller of types suitable for application.

#### Work paint into cracks, crevices and corners.

#### Paint surfaces and corners not accessible to brush using spray, daubers and/or sheepskins.  Paint surfaces and corners not accessible to roller using brush, daubers or sheepskins.

#### Brush and/or roll out runs and sags, and over-lap marks.  Rolled surfaces to be free of roller tracking and heavy stipple.

#### Remove runs, sags and brush marks from finished work and repaint.

### Spray Application:

#### Provide and maintain equipment that is suitable for intended purpose, capable of properly atomizing paint to be applied, and equipped with suitable pressure regulators and gauges.

#### Keep paint ingredients properly mixed in containers during paint application either by continuous mechanical agitation or by intermittent agitation as frequently necessary.

#### Apply paint in a uniform layer, with overlapping at edges of spray pattern.

#### Back roll spray applications and brush out runs and sags immediately.

#### Use brushes to work paint into cracks, crevices and places that are not adequately painted by spray.

### Use dipping, sheepskins or daubers when no other method is practical in places of difficult access and when specifically authorized by Owner.

### Apply paint coats in a continuous manner and allow surfaces to dry and properly cure between coats for minimum time period as recommended by manufacturer.  Minimum dry film thickness of coats shall not be less than that recommended by the manufacturer.  Repaint thin spots or bare areas before next coat of paint is applied.

### Sand and dust between coats to remove visible defects.

### Finish surfaces both above and below sight lines as specified for surrounding surfaces, including such surfaces as projecting ledges.

### Finish to doors shall include all edges including top and bottom edges.  Surfaces concealed by door hardware shall also be repainted unless otherwise pre-approved.

## MECHANICAL / ELECTRICAL EQUIPMENT

### Unless otherwise noted, repainting shall also include exposed to view/previously painted exterior mechanical and electrical equipment and components (panels, conduits, piping, hangers, ductwork, etc.).

### Touch up scratches and marks and repaint such mechanical and electrical equipment and components with colour and finish to match existing finish unless otherwise noted or scheduled.

### Do not paint over name plates or instruction labels.

## FIELD QUALITY CONTROL

### Field inspection of exterior painting operations to be carried out by Owner.

### Advise Owner when each surface and applied coating is ready for inspection.  Do not proceed with subsequent coats until previous coat has been approved.

### Co-operate with Owner and provide access to areas of work.

## CLEAN-UP

### Remove paint where spilled, splashed, splattered or sprayed as work progresses using means and materials that are not detrimental to affected surfaces.

### Keep work area free from an unnecessary accumulation of tools, equipment, surplus materials and debris.

### Remove combustible rubbish materials and empty paint cans each day and safely dispose of same in accordance with requirements of authorities having jurisdiction.

### Clean equipment and dispose of wash water used for water borne materials, solvents used for oil based materials as well as cleaning and protective materials (e.g. rags, drop cloths, masking papers, etc.), paints, thinners, paint removers / strippers in accordance with the safety requirements of authorities having jurisdiction and as noted herein.

### Painting equipment shall be cleaned in leak-proof containers that will permit particulate matter to settle out and be collected.  Sediment remaining from cleaning operations shall be disposed of in a manner acceptable to authorities having jurisdiction.

### Paint and coatings in excess of repainting requirements shall be recycled as noted herein.

## RESTORATION

### Clean and re-install hardware items removed before undertaken painting operations.

### Remove protective coverings and warning signs as soon as practical after operations cease.

### Remove paint splashings on affected exposed surfaces.  Remove smears and spatter immediately as operations progress, using compatible solvent.

### Protect freshly completed surfaces from paint droppings and dust to approval of Owner.  Avoid scuffing newly applied paint.

### Restore areas used for storage, cleaning, mixing and handling of paint to clean condition as approved by Owner.

END OF SECTION