GENERAL

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 01 43 39 – Mock Up Requirements.

### Section 01 61 00 - Common Product Requirements.

### Section 01 74 21 - Construction/Demolition Waste Management and Disposal.

### Section 01 78 00 - Closeout Submittals.

### Section 07 92 00 - Joint Sealants.

### Section 09 21 16 – Gypsum Board Assemblies.

### Section 10 28 10 – Toilet and Bath Accessories.

## REFERENCES

### American National Standards Institute (ANSI)/Ceramic Tile Institute (CTI)

#### ANSI A108.1, Specification for the Installation of Ceramic Tile (Includes ANSI A108.1A-C, 108.4-.13, A118.1-.10, ANSI A136.1).

#### CTI A118.6, Specification for Ceramic Tile Grouts (included in ANSI A108.1).

### American Society for Testing and Materials (ASTM)

#### ASTM C144, Specification for Aggregate for Masonry Mortar.

#### ASTM C207, Specification for Hydrated Lime for Masonry Purposes.

### Canadian General Standards Board (CGSB)

#### CAN/CGSB-51.34, Vapour Barrier, Polyethylene Sheet for Use in Building Construction.

#### CGSB 71-GP-22M, Adhesive, Organic, for Installation of Ceramic Wall Tile.

#### CAN/CGSB-75.1, Tile, Ceramic.

#### CAN/CGSB-25.20, Surface Sealer for Floors.

### Canadian Standards Association (CSA)

#### CAN/CSA-A3000, Cementitious Materials Compendium (Consists of A5, A8, A23.5, A362, A363, A456.1, A456.2, A456.3).

### Terrazzo Tile and Marble Association of Canada (TTMAC)

#### Tile Specification Guide 09300, Tile Installation Manual.

#### Tile Maintenance Guide

## SUBMITTALS

### Include manufacturer's information on:

#### Ceramic tile, marked to show each type, size, and shape required.

#### Dry-set Portland cement mortar and grout.

#### Divider strip.

#### Reinforcing tape.

#### Levelling compound.

#### Waterproofing isolation membrane.

### Submit duplicate 300 x 300 mm sample panels of each colour, texture, size, and pattern of tile.

### Trim shapes, bullnose cap and cove including bullnose cap and base pieces at internal and external corners of vertical surfaces, each type, colour, and size.

### Adhere tile samples to 11 mm thick plywood and grout joints to represent project installation.

## DELIVERY, STORAGE AND HANDLING

### Deliver, store, handle and protect materials in accordance with Section 01 61 00 – Common Product Requirements.

### Deliver, store and handle products in a manner to avoid damage or contamination.

### Have materials delivered to job site prior to installation.

### Deliver all products to job site in manufacturer’s unopened cartons with all labels intact and legible.

### Keep cartons dry and protect from vandalism and away from heavy traffic area.

### Store cartons in upright position.

## ENVIRONMENTAL CONDITIONS

### Maintain air temperature and structural base temperature at ceramic tile installation area above 12° C for 48 h before, during, and 48 h after, installation.

### Do not install tiles at temperatures less than 12° C or above 38°C.

### Do not apply epoxy mortar and grouts at temperatures below 15° C or above 25° C.

## QUALIFICATIONS

### Tile setters: Minimum 5 years proven experience.

## MOCK-UP

### Construct mock-ups in accordance with Section 01 43 39 – Mock Up Requirements.

## QUALITY ASSURANCE

### Provide certificate of quality compliance from tile manufacturer.

### Provide certificate of quality compliance from tile installer upon satisfactory completion of installation.

PRODUCTS

## FLOOR TILE

### Ceramic tile: to CAN/CGSB-75.1, Type 7, Class MR I, size as indicated on drawings, square edges, slip resistant surface, colour as selected by Owner. Matching coved base, size as indicated on drawings.

## WALL TILE

### Ceramic tile: to CAN/CGSB-75.1, Type 5, Class MR 4, size as indicated on drawings, rounded edges, glazed surface, colour as selected by Owner. Matching bullnose edge trim to suit application.

## TRIM SHAPES

### Conform to applicable requirements of adjoining floor and wall tile.

### Use trim shapes sizes conforming to size of adjoining field wall tile, including existing spaces, unless specified otherwise.

## MORTAR AND ADHESIVE MATERIALS

### Portland cement: to CSA-A5, type 10.

### Sand: to ASTM C144, passing 16 mesh.

### Hydrated lime: to ASTM C207, Type N.

### Latex additive: formulated for use in portland cement mortar and thin set bond coat.

### Water: potable and free of minerals and chemicals which are detrimental to mortar and grout mixes.

### Dry set mortar: to ANSI A118.1.

## GROUT

### Portland cement grout: as recommended by tile manufacturer.

### Dry curing wall grout: as recommended by tile manufacturer.

### Grout preparation: to manufacturer’s instructions.

### Colouring Pigments:

#### Pure mineral pigments, limeproof and nonfading, complying with ASTM C979.

#### Colouring pigments to be added to grout by manufacturer.

#### Job coloured grout are not acceptable.

## ACCESSORIES

### Thresholds: marble, 12 mm thick, rounded edges two sides, honed finish to exposed surfaces, size to suit door opening and frame width.

### Sealant: acrylics one part, mildew resistant, in accordance with Section 07 92 00 - Joint Sealants.

### Floor sealer and protective coating: to tile and grout manufacturer’s recommendations.

## MORTAR AND ADHESIVE MIXES

### Mortar bed for floors: 1 part Portland cement, 4 parts sand, 1 part water. Adjust water volume depending on water content of sand. Latex additive may be included.  Mortar bed for walls 1 part portland cement, 1/5 Dry set mortar: mix to manufacturer's instructions.

### Organic adhesive: pre-mixed.

### Mix bond and levelling coats, and grout to manufacturer's instructions.

### Adjust water volumes to suit water content of sand.

## CLEANING COMPOUNDS

### Specifically designed for cleaning masonry and concrete and which will not prevent bond of subsequent tile setting materials including patching and leveling compounds and elastomeric waterproofing membrane and coat.

### Materials containing acid or caustic material are not acceptable.

EXECUTION

## WORKMANSHIP

### Do tile work in accordance with TTMAC Tile Installation Manual, “Ceramic Tile”, latest edition.

### Apply tile to clean and sound surfaces.

### Fit tile around corners, fitments, fixtures, drains and other built-in objects. Maintain uniform joint appearance. Cut edges smooth and even. Do not split tiles.

### Maximum surface tolerance 1:800.

### Make joints between tile uniform and approximately 1.5 mm wide, plumb, straight, true, even and flush with adjacent tile. Ensure sheet layout not visible after installation. Align patterns.

### Lay out tiles so perimeter tiles are minimum 1/2 size.

### Sound tiles after setting and replace hollow-sounding units to obtain full bond.

### Make internal angles square, external angles bullnosed.

### Use bullnose edged tiles at termination of wall tile panels, except where panel abuts projecting surface or differing plane.

### Install divider strips at junction of tile flooring and dissimilar materials.

### Allow minimum 24 h after installation of tiles, before grouting.

### Clean installed tile surfaces after installation and grouting cured.

### Make control joints where indicated. Make joint width same as tile joints. Fill control joints with sealant in accordance with Section 07 92 00 - Joint Sealants. Keep building expansion joints free of mortar and grout.

## WALL TILE

### Install in accordance with TTMAC details 302W-2002, 303W-2002, 305W-2002.

## FLOOR TILE

### Install in accordance with TTMAC detail 311F-2002.

## FLOOR SEALER AND PROTECTIVE COATING

### Apply in accordance with manufacturer's instructions.

## COMMISSIONING

### Train user staff in the care and cleaning of ceramic tile and in the application of sealers.

### Train user staff in the repair and or replacement of damaged tiles.

END OF SECTION