# GENERAL

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

### Section 01 78 00 - Closeout Submittals.

## REFERENCES

### American Society for Testing and Materials (ASTM)

#### ASTM F1066, Specification for Vinyl Composition Floor Tile.

### Canadian General Standards Board (CGSB)

#### CAN/CGSB-25.20, Surface Sealer for Floors.

#### CAN/CGSB-25.21, Detergent-Resistant Floor Polish.

## SUBMITTALS

### Submit duplicate tile in size specified, 300 mm long base.

## CLOSEOUT SUBMITTALS

### Provide maintenance data for resilient flooring for incorporation into manual specified in Section 01 78 00 - Closeout Submittals.

## ENVIRONMENTAL REQUIREMENTS

### Maintain air temperature and structural base temperature at flooring installation area at 18º C to 30º C for 48 hours before, during and for 48 hours after installation, and at relative humidity not greater than 60%.

## WARRANTY

### Flooring materials shall be warranted by the manufacturer against defects in materials and workmanship for a period of five (5) years from the date of Substantial Completion.

### Contractor shall provide a two (2) year warranty from the date of substantial completion against defects in workmanship.

# PRODUCTS

## MATERIALS

### Resilient flooring must:

#### Meet or exceed all applicable governmental and industrial safety and performance standards; and

#### Be manufactured and transported in such a manner that all steps of the process, including the disposal of waste products arising therefrom, will meet the requirements of all applicable governmental acts, by laws and regulations including, for facilities located in Canada, the Fisheries Act and the Canadian Environmental Protection ct (CEPA)

### Vinyl composition tile (VCT): to ASTM F1066, Composition 1 - non asbestos Class 2 - through pattern tile, plain surface, minimum 3.0 mm thick, minimum 305 mm x 305 mm unless otherwise indicated, in colour selected by Owner.

### Linoleum Tile: renewable, polymer based floor tile having a nominal total thickness of minimum 2.0 mm, minimum 305 mm x 305 mm unless otherwise indicated, composed of polyester resin and fillers. Pigment with colours and textures to be dispersed uniformly throughout total thickness.

### Vinyl flooring must:

#### Floor tile to confirm to ASTM F1066, Class 2 – through pattern, for size, squareness, thickness, indentation, impact, deflection, resistance to chemicals and resistance to heat.

#### Not be manufactured or formulated with cadium (Cd), chromium (Cr), lead (Pb,), mercury (Gg), and nickel (Ni);

#### Not contain >0.01% by weight of arsenic (As);

#### Not contain >1% by weight of tin (Sn), or zinc (Zn);

#### Not be manufactured or formulated with short-chained chlorinated paraffin waxes (CS≤13), or nonyl phenol;

#### Not contain or be manufactured with materials derived from species listed on the Convention on International Trade in Endangered Species (CITES).

### Feature strip: of same material and thickness as adjacent work, width as indicated on drawings, colour as selected by Owner.

### Resilient base: rubber, coved, minimum 1200 mm length and 101.6 mm high x 2.0 mm thick, including external corners for coved base only, of colour selected by Owner.

### Primers and adhesives: waterproof, solvent-free, recommended by flooring manufacturer for specific material on applicable substrate, above, at or below grade.

### Sub-floor filler and leveller: white premix latex requiring water only to produce cementitious paste as recommended by flooring manufacturer for use with their product.

### Metal edge strips: aluminum extruded, smooth, mill finish with lip to extend under floor finish, shoulder flush with top of adjacent floor finish.

### Sealer: to CAN/CGSB 25.20M, type recommended by flooring manufacturer.

### Wax: to CAN/CGSB-25.21 type recommended by flooring manufacturer.

# EXECUTION

## INSPECTION

### Ensure concrete floors are dry, by using test methods recommended by tile manufacturer.

## SUB-FLOOR TREATMENT

### Remove all tile adhesive from existing floor areas to receive new tile.

### Remove floor ridges and bumps. Fill low spots, cracks, joints, holes and other defects with floor filler.

### Clean floor and apply filler; trowel and float to leave smooth, flat hard surface. Prohibit traffic until filler cured and dry.

### Old vinyl flooring to be removed by trained personnel (may contain asbestos).

### Remove or treat old adhesives to prevent residual, old flooring adhesives from bleeding through to new flooring and/or interfering with the bonding of new adhesives.

## TILE APPLICATION

### Provide a high ventilation rate, with maximum outside air, during installation, and for 48 to 72 hours after installation. If possible, vent directly to the outside. Do not let contaminated air recirculate through a district or whole building air distribution system. Upon completion of work, maintain ventilation at maximum capacity until building occupation.

### To minimize emissions from adhesives, use water-based, solvent-free styrene-butadiene-rubber adhesive for linoleum. Butadiene exposure may cause eye and nose irritations, headaches, dizziness, and vomiting.

### Apply adhesive uniformly using recommended trowel in accordance with flooring manufacturer's instructions. Do not spread more adhesive than can be covered by flooring before initial set takes place.

### Lay flooring with joints parallel to building lines to produce symmetrical tile pattern. Border tiles minimum half tile width.

### Install flooring to square grid pattern with all joints aligned, with pattern grain alternating to produce basket weave pattern.

### As installation progresses, and after installation, roll flooring in 2 directions including resilient tile with 45 kg minimum roller to ensure full adhesion.

### Cut tile and fit neatly around fixed objects.

### Install feature strips and floor markings where indicated. Fit joints tightly.

### Install flooring in pan type floor access covers. Maintain floor pattern.

### Continue flooring through areas to receive movable type partitions without interrupting floor pattern.

### Terminate flooring at centreline of door in openings where adjacent floor finish or colour is dissimilar.

### Install metal edge strips at unprotected or exposed edges where flooring terminates.

## BASE APPLICATION

### Lay out base to keep number of joints at minimum. Base joints at maximum length available or at internal or premoulded corners.

### Clean substrate and prime with one coat of adhesive.

### Apply adhesive to back of base.

### Set base against wall and floor surfaces tightly by using 3 kg hand roller.

### Install straight and level to variation of 1:1000.

### Scribe and fit to door frames and other obstructions.

### Cope internal corners. Use premoulded corner units for right angle external corners. Use formed straight base material for external corners of other angles, minimum 300 mm each leg. Wrap around toeless base at external corners.

## INITIAL CLEANING AND WAXING

### Remove excess adhesive from floor, base and wall surfaces without damage.

### Clean, seal and wax floor and base surface to flooring manufacturer's instructions. In carpeted areas clean, seal and wax base surface before carpet installation.

## PROTECTION OF FINISHED WORK

### Protect new floors after initial waxing until final inspection.

### Prohibit traffic on floor for 48 hours after installation.

END OF SECTION