# GENERAL

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 01 43 39 – Mock Up Requirements.

### Section 01 74 00 – Cleaning.

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

### Section 01 78 00 - Closeout Submittals.

## REFERENCES

### American Society for Testing and Materials (ASTM)

#### ASTM F1303, Specification for Sheet Vinyl Floor Covering with Backing.

## SUBMITTALS

### Submit duplicate 300 x 300 mm sample pieces of sheet material, 300 mm long base, feature strips, edge strips.

## CLOSEOUT SUBMITTALS

### Provide maintenance data for safety flooring for incorporation into manual specified in Section 01 78 00 - Closeout Submittals.

## ENVIRONMENTAL REQUIREMENTS

### Maintain air temperature and structural base temperature at flooring installation area at 15º C for 24 hours before, during and 24 hours after installation, and at a relative humidity not greater than 60%.

## QUALIFICATIONS

### Safety Sheet flooring installers: minimum 5 years proven experience.

## MOCK-UP

### Construct mock-ups when requested in accordance with Section 01 43 39 – Mock Up Requirements.

## QUALITY ASSURANCE

### Provide Certificate of Quality Compliance from sheet flooring manufacturer.

### Provide Certificate of Quality Compliance from flooring installer upon satisfactory completion of installation.

## Warranty

### Flooring materials shall be warranted by the manufacturer against defects in materials and workmanship for a period of ten (10) years from the date of Substantial Completion.

### Contractor shall provide a two (2) year warranty from the date of substantial completion against defects in workmanship.

# PRODUCTS

## MATERIALS

### Safety flooring must:

#### Meet or exceed all applicable governmental and industrial safety and performance standards; and

#### Be manufactured and transported in such a manner that all steps of the process, including the disposal of waste products arising therefrom, will meet the requirements of all applicable governmental acts, by laws and refulatons including, for facilities located in Canada, the Fisheries Act and the Canadian Environmental Protection Act (CEPA).

### Safety sheet vinyl with backing: to ASTM F1303.

#### Slip resistant, multicolored chip design, inlaid with carborundum particles.

#### Type I.

#### Grade: 1.

#### Backing: non-woven glassfibre grid, to ASTM F1303-99, Class B.

#### Pattern: shall extend uniformly through entire thickness of wearlayer.

#### Colour: selected by Owner.

#### Thickness: 2.0 mm.

#### Wearlayer: 1.0 mm.

#### Flooring shall be supplied in rolls of uniform thickness 2.0 m wide by 20 m long minimum.

#### Weight: 2.7 kg/m2.

#### Fire rating: ≥ 0.45, to ATSM E 648.

#### Electrical resistance: ≤ 2 kV, to DIN 54 345.

#### Slip resistance: R10, to DIN 51 130.

#### Chemical Resistance: to EN 423, floor to be resistant to the following chemicals in diluted form:

##### Acetic Acid

##### Acetone

##### Alcohol (ethanol 95%)

##### Alcohol (methyl)

##### Ammonium Oxalate

##### P-Dimethylaminobenzaldehyde

##### Ferric Chloride

##### Hydrochloric Acid

##### Hydrogen Peroxide

##### Indole Reagent

##### Iodine

##### Naphthol

##### Ninhydrin

##### Oxalic Acid

##### Phenol

##### Potassium Hydroxide

##### Potassium Iodide

##### Potassium Permanganate

##### Sodium Hydroxide

##### Sulfuric Acid

##### Zinc Sulfate

##### TRA

##### Methyl Red

### Resilient base: continuous, top set, complete with premoulded end stops and external corners:

#### Type: rubber

#### Style: cove

#### Thickness: 2.03 mm.

#### Height: 101.6 mm.

#### Lengths: cut lengths minimum 1200 mm.

#### Colour: selected by Owner.

### Primers and adhesives: of types recommended by safety sheet flooring manufacturer for specific material on applicable substrate, above, on or below grade.

### Sub-floor filler and leveller: white premix latex requiring water only to produce cementitious paste as recommended by flooring manufacturer for use with their product.

### Metal edge strips:

#### Aluminum extruded, smooth, with lip to extend under floor finish, shoulder flush with top of adjacent floor finish.

# EXECUTION

## PREPARATION

### Concrete floor slab must be smooth and level and be within tolerance of + 3 mm in 3 m radius.  Remove ridges and bumps.  Fill low spots, cracks, joints, holes and other defects with an approved filler.  Remove any other contaminants such as grease, paint, dust, solvents or rust.

### Moisture vapour emission content of the concrete floor slab shall not exceed 1.46 kg/100 m2 per 24 hours when using the calcium chloride test method moisture vapour emission content prior to safety sheet flooring installation in new construction. Any corrective measures are the responsibility of the contractor.  In the case of existing facilities where the safety sheet flooring is being replaced, the flooring supplier is to provide a flooring system suitable for the existing moisture vapour emission content as determined by the flooring supplier during the tender period.

### Remove or treat old adhesives to prevent residual, old flooring adhesives from bleeding through to new flooring and/or interfering with the bonding of new adhesives.

### Seal concrete slab or plywood sub-floor to safety flooring manufacturer's printed instructions.

## APPLICATION: FLOORING

### Provide a high ventilation rate, with maximum outside air, during installation, and for 48 to 72 hours after installation. If possible, vent directly to the outside. Do not let contaminated air recirculate through a district or whole building air distribution system. Upon completion of work, maintain ventilation at maximum capacity until building occupation.

### To minimize emissions from adhesives, use water-based, solvent-free styrene-butadiene-rubber adhesive for linoleum. Butadiene exposure may cause eye and nose irritation, headaches, dizziness, and vomiting.

### Apply water based adhesive uniformly using recommended trowel. Do not spread more adhesive than can be covered by flooring before initial set takes place.

### Lay flooring with seams parallel to building lines to produce a minimum number of seams. Border widths minimum 1/3 width of full material.

### Run sheets in direction of traffic. Double cut sheet joints and continuously heat weld according to manufacturer's printed instructions.

### Heat weld seams of safety sheet flooring in accordance with manufacturer's printed instructions.

### As installation progresses, and after installation roll flooring with 65 kg minimum roller to ensure full adhesion.

### Cut flooring neatly around fixed objects.

### Install feature strips and floor markings where indicated. Fit joints tightly.

### Install flooring in pan type floor access covers. Maintain floor pattern.

### Continue flooring over areas which will be under built-in furniture.

### Continue flooring through areas to receive movable type partitions without interrupting floor pattern.

### Terminate flooring at centreline of door in openings where adjacent floor finish or colour is dissimilar.

### Install metal edge strips at unprotected or exposed edges where flooring terminates.

## APPLICATION: BASE

### Lay out base to keep number of joints at minimum.

### Clean substrate and prime with one coat of adhesive.

### Apply adhesive to back of base.

### Set base against wall and floor surfaces tightly by using 3 kg hand roller.

### Install straight and level to variation of 1:1000.

### Scribe and fit to door frames and other obstructions. Use premoulded end pieces at flush door frames.

### Cope internal corners. Use premoulded corner units for right angle external corners. Use formed straight base material for external corners of other angles.

### Heat weld base in accordance with manufacturer's printed instructions.

## CLEANING

### Remove excess adhesive from floor, base and wall surfaces without damage.

### Clean, seal and apply 2 coats of an approved floor wax plus one wear layer of floor wax to flooring and base surface in accordance with manufacturer's instructions.

## PROTECTION

### Prohibit traffic on floor for 48 hours after installation.

### Protect new floors from time of final set of adhesive until substantial inspection and to handover of completed project.

## COMMISSIONING

### Train area staff in the care, cleaning and sealing of resilient sheet flooring.

### Acceptance of maintenance material turned over to owner.

END OF SECTION