# GENERAL

## RELATED WORK

### Section 01 33 00 - Submittal Procedures.

### Section 01 43 39 – Mock Up Requirements.

### Section 01 45 00 - Quality Control.

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

### Section 06 10 53 – Miscellaneous Rough Carpentry.

### Section 10 28 10 - Toilet and Bath Accessories.

## REFERENCES

### American Society for Testing and Materials (ASTM)

#### ASTM A167, Specification for Stainless and Heat-Resisting Chromium-Nickel Steel Plate, Sheet, and Strip.

#### ASTM A480/A480M, Specification for General Requirements for Flat-Rolled Stainless and Heat Resisting Steel Plate, Sheet and Strip.

### Canadian General Standards Board (CGSB)

#### CAN/CGSB-1.81, Air Drying and Baking Alkyd Primer for Vehicles and Equipment.

#### CAN/CGSB-1.88, Gloss Alkyd Enamel, Air Drying and Baking.

#### CAN/CGSB-1.104M, Semigloss Alkyd, Air Drying and Baking Enamel.

### Canadian Standards Association (CSA)

#### CSA B651, Accessible Design for the Built Environment.

## SUBMITTALS

### Submit 300 x 300 mm samples of panel showing finished edge and corner construction and core construction.

### Submit representative samples of each hardware item, including brackets, fastenings and trim.

### Indicate fabrication details, plans, elevations, hardware, and installation details.

### Submit manufacturer's printed product literature, specifications and data sheet.

### Submit two copies of WHMIS SDS - Safety Data Sheets. Indicate VOC's:

#### For caulking materials during application and curing.

### Submit manufacturer’s installation instructions.

## MOCK-UPS

### Construct mock-ups in accordance with Section 01 43 39 – Mock Up Requirements.

### Locate where directed.

# PRODUCTS

## MATERIALS

### Metal toilet partitions.

### Sheet steel: commercial quality to ASTM A480/480M with ZF001 designation zinc coating.

### Minimum base steel thickness:

#### Panels and doors: 0.8 mm.

#### Pilasters: 1.0 mm.

#### Reinforcement: 3.0 mm.

### Stainless steel sheet metal: to ASTM A167, Type 304 with BA finish.

### Headrails: 25 mm x 41 mm x 1.5 mm thick, clear anodized, extruded aluminum, anti grip design.

### Pilaster shoe: 0.8 mm stainless steel, 75 mm high.

### Attachment: stainless steel tamperproof type screws and bolts.

## COMPONENTS

### Hinges:

#### Heavy duty, non-lubricating nylon bushings.

#### Material/finish: chrome plated non-ferrous casting.

#### Swing: inward and outward for barrier free.

#### Return movement: gravity.

#### Adjustable to hold door open at any angle up to 90°.

#### Emergency access feature.

### Latch set: built-in, combination latch, door-stop, keeper and bumper, chrome plated non-ferrous.

### Wall and connecting brackets: chrome plated non-ferrous extrusion or casting.

### Coat hook: combination hook and rubber door bumper, chrome plated non-ferrous.

### Door pull: Barrier-free type suited for outswinging doors, chrome plated non-ferrous.

## FABRICATION

### Doors, panels and screens: 25 mm thick, two steel sheets faces pressure bonded to honeycomb core, to sizes indicated.

### Pilasters: 32 mm thick, constructed same as door, to sizes indicated.

### Provide formed and closed edges for doors, panels and pilasters. Miter and weld corners and grind smooth.

### Provide internal reinforcement at areas of attached hardware and fittings. Temporarily mark location of reinforcement for tissue holders and grab bars.

## FINISHES

### Clean, degrease and neutralize steel components with phosphate or chromate treatment.

### Spray apply primer to CAN/CGSB-1.81, 1 coat.

### Spray apply finish enamel to CGSB 1-GP-104, Type 2, semi-gloss, 2 coats and bake to smooth, hard finish 0.025 mm thick.

### Finish: doors and pilaster/panels as selected from manufacturer's standard colours.

# EXECUTION

## MANUFACTURER'S INSTRUCTIONS

### Compliance: comply with manufacturer's written data, including product technical bulletins, product catalogue installation instructions, product carton installation instructions, and data sheets.

## INSTALLATION

### Ensure supplementary anchorage, if required, is in place.

### Do work in accordance with CAN/CSA-B651.

## ERECTION

### Partition erection:

#### Install partitions secure, plumb and square.

#### Leave 12 mm space between wall and panel or end pilaster.

#### Anchor mounting brackets to masonry/concrete surfaces using screws and shields: to hollow walls using bolts and toggle type anchors, to steel supports with bolts in threaded holes.

#### Attach panel and pilaster to brackets with through type sleeve bolt and nut.

#### Provide for adjustment of floor variations with screw jack through steel saddles made integral with pilaster. Conceal floor fixings with stainless steel shoes.

#### Equip each door with hinges, latch set, and each stall with coat hook mounted on door, mounting heights 1550 mm.  Adjust and align hardware for easy, proper function. Set door open position at full open.

#### Equip outswinging doors with door pulls on inside and outside of door in accordance with CAN/CSA-B651.

#### Install hardware and grab bars.

### Floor supported and headrail braced partition erection.

#### Attach pilasters to floor with pilaster supports and level, plumb, and tighten installation with levelling device.

##### Secure pilaster shoes in position.

##### Secure headrail to pilaster face with not less than two fasteners per face.

##### Set tops of doors parallel with overhead brace when doors are in closed position.

### Screens erection.

#### Provide urinal stall screens consisting of panel, pilaster and headrail as specified for toilet compartments.

#### Anchor screen panels to walls with 3 panel brackets, and pilaster complete with floor shoes, anchored to floor.

## ADJUSTING

### Adjust doors and locks for optimum, smooth operating condition.

### Lubricate hardware and other moving parts.

## CLEANING

### Perform cleaning after installation to remove construction and accumulated environmental dirt.

### Clean surfaces after installation using manufacturer's recommended cleaning procedures.

### Clean aluminum with damp rag and approved non-abrasive cleaner.

### Clean and polish hardware and stainless components.

### Upon completion of installation, remove surplus materials, rubbish, tools and equipment barriers.

END OF SECTION