# GENERAL

## RELATED SECTIONS

### Section 01 33 00 – Submittal Procedures.

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

### Section 06 10 53 – Miscellaneous Rough Carpentry.

## REFERENCES

### Aluminum Association (AA)

#### DAF 45, Designation System for Aluminum Finishes.

## SUBMITTALS

### Product Data

#### Submit manufacturers printed product literature, specifications and data.

#### Submit two copies of WHMIS SDS –Safety Data Sheets. Indicate VOC’s:

##### For caulking materials during application and curing.

##### For adhesives.

### Indicate, by large scale details, all materials, finishes, dimensions, anchorage and assembly.

### Submit 300 mm long samples of profiles and colours for corner and door frame and wall guards.

### Manufacturer’s Instructions

#### Submit manufacturer’s installation instructions

# PRODUCTS

## MATERIALS

### Vinyl corner guard: 76 mm x 76 mm x 1.98 mm thick, 1200 mm length, complete with end caps to match guard material, mechanically or adhesive mounted, color as selected by Owner.  Locations as indicated on drawings.

### Wall bumper guard:  vinyl to profiles indicated, complete with end caps to match wall bumper guard material, surface mechanically or adhesive mounted, colour as selected by Owner.  See finish schedule and drawings for heights and locations.

### Door frame bumper guards:  vinyl, profiled to fit door frame, colour selected by Owner. Model to fit door frame style. See door schedule for locations.

## ACCESSORIES

### Fasteners: self-tapping stainless steel, concealed flush mounting.

### Adhesive: water resistant type as recommended by manufacturer for substrate.

## FINISHES

### Finish exposed surfaces of aluminum components in accordance with Aluminum Designation System for Aluminum Finishes.

### Appearance and properties of anodized finishes designated by the Aluminum Association as Architectural Class 1, Architectural Class 2, and Protective and Decorative.

# EXECUTION

## MANUFACTURER’S INSTRUCTIONS

### Compliance: comply with manufacturer’s written data, including product technical bulletins, product catalogue installation instructions, product carton installation instructions, and data sheets.

## INSTALLATION

### Install units on solid wood backing and erect with materials and components straight, tight and in alignment.

### Mechanically fasten/adhere wall guards at 200 mm on centre as indicated, straight and level to variation plus or minus 3.0 mm over 3000 mm straight edge, non-cumulative.

### Mechanically fasten/adhere corner guards at 200 mm on centre as indicated.

## CLEANING

### Perform cleaning after installation to remove construction and accumulated environmental dirt.

### Clean surfaces after installation using manufacturer’s recommended cleaning procedures.

### Upon completion of installation, remove surplus materials, rubbish, tools and equipment barriers.

#### Provide Owner with instructions on cleaning.

END OF SECTION