# GENERAL

## SECTIONS INCLUDES

### Materials, fabrications and installation for, aluminum flagpoles.

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 01 61 00 - Common Product Requirements.

### Section 01 74 21 – Construction/Demolition Waste Management and Disposal.

### Section 03 10 00 - Concrete Forming and Accessories.

### Section 03 30 00- Cast-in-Place Concrete.

### Section 06 10 53 – Miscellaneous Rough Carpentry.

### Section 31 23 33.01 - Excavating, Trenching and Backfilling.

## REFERENCES

### The Aluminum Association (AA)

#### DAF 45, Designation System for Aluminum Finishes.

### American Society for Testing and Materials International (ASTM)

#### ASTM B241/B241M, Standard Specification for Aluminum and Aluminum - Alloy Seamless Pipe and Seamless Extruded Pipe.

### The Masters Painters Institute (MPI)

#### Architectural Painting Specification Manual.

## DESIGN REQUIREMENTS

### Flagpole, bases and anchorage devices to resist minimum wind velocity of 145 km/h unflagged, 100 km/h flagged.

## SUBMITTALS

### Submit manufacturer’s technical data and installation instructions for each type of flagpole.

### Indicate dimensions, finishes, base jointing, anchoring and support systems, cleats, halyard boxes, trucks, finials, and base collar for flagpoles.

### Submit Shop Drawings of flagpoles and bases, showing general layout, jointing and complete anchoring and supporting systems.

### Submit sample of flagpole 900 mm long.

## QUALITY ASSURANCE

### Provide each flagpole as complete unit produced by single manufacturer, including fittings, accessories, bases and anchorage devices.

## DELIVERY AND STORAGE

### Deliver, store, handle and protect materials in accordance with Section 01 61 00 - Common Product Requirements.

### Spiral wrap each flagpole with heavy kraft paper, wood strip and steel band, or polyethylene wrap and pack in tubing for shipment.

# PRODUCTS

## MATERIALS

### Aluminum: Aluminum Association alloy AA 6063-T5 seamless extruded aluminum tubing.

### Isolation coating: alkali-resistant bituminous paint or epoxy resin solution.

## FABRICATION

### Supply (fill in length) mm long flagpole as complete unit including base, mounting brackets, anchorage and fittings.

### Cone tapered flagpole:

#### Seamless, uniform, straight line tapered section above cylindrical butt section.

#### Taper: 25 mm of run.

#### Provide internal splicing, self-aligning sleeve of same material as flagpole for snug fitting, watertight field joints.

### Do welding to appropriate CSA Standards by welders certified by Canadian Welding Bureau.  Finish exposed welds flush and smooth.

## ACCESSORIES

### Finial: 150 mm diameter ball of 1.6 mm minimum thick, aluminum, anodized to match flagpole finish.

### Truck assembly: cast aluminum, stainless steel ballbearing, nonfouling, revolving double truck assembly, finish to match flagpole.

### Cleats: 230 mm size, two per halyard, cast aluminum, finish to match flagpole.

### Halyard: internal, two continuous halyards per flagpole; 10 mm (No. 12) polypropylene, braided white cotton. Retaining loop and weights for internal halyard, stainless steel.

### Swivel snaps: two per halyard; aluminum with neoprene or vinyl covers.

### Cleat box: one per cleat; cast aluminum, finish to match flagpole. Furnish hasp for padlock, hinged cover, and tamperproof screws. Include lockable cleat box.

## FINISHES

### Finish exposed surfaces of aluminum components in accordance with Aluminum Association Designation System for Aluminum Finishes.

#### Clear anodic finish: designation AA-M32, C22, A41.

### Appearance and properties of anodized finishes designated by the Aluminum Association as Architectural Class 1, Architectural Class 2, and Protective and Decorative.

## FIELD FABRICATION

### Fabricate ground-set foundation assembly for sleeve installation of flagpole as recommended by Flagpole manufacturer for wind loads as indicated.

# EXECUTION

## INSTALLATION

### Shop apply isolation coating to metal surfaces of flagpole and base that will be encased in concrete.

### Install flagpoles, base assemblies and fittings to shop drawings and manufacturer's instructions.

### Provide lightning rods for grounding of each flagpole installation as indicated.

## Commissioning

### Check and adjust installed fittings for smooth operation of halyards, and instruct Owner on adjustment and maintenance procedures.

END OF SECTION