# General

## RELATED SECTIONS

### Section 01 33 00 - Submittal Procedures.

### Section 03 30 00 - Cast-in-Place Concrete.

### Section 05 50 00 - Metal Fabrications.

### Section 09 91 13 - Exterior Painting.

## REFERENCES

### American Society for Testing and Materials (ASTM)

#### ASTM D624, Standard Test Method for Tear Strength of Conventional Vulcanized Rubber and Thermplastic Elastomers.

#### ASTM D1171, Standard Test Method for Rubber Deterioration-Surface Ozone Cracking Outdoors or Chamber.

#### ASTM D2632, Standard Test Method for Rubber Property-Resilience by Vertical Rebound.

## SUBMITTALS

### Indicate:

#### Dimensions and required clearances.

#### Fastening methods for dock bumpers.

### Submit samples of:

#### 300 mm long sections of dock bumpers.

# Products

## MANUFACTURED UNITS

### Laminated Dock Bumper

#### Rubber pads laminated between structural steel angles and compressed under approximately 680 kg pressure. 178 mm x 140 mm x 508 mm steel angles welded to 19 mm steel rods at one end and closed with threaded rod and nut at other end.

#### Anchor leg of angle extends 76 mm beyond rubber surface at each end and contains three 21 mm anchor bolt holes as required.

#### Hot-dipped galvanized finish for exposed metal parts.

# Execution

## INSTALLATION

### No assembly required for pre-manufactured unit. Install dock bumper in accordance with manufacturer’s instructions and as indicated.

END OF SECTION