# GENERAL

## SUMMARY

### This Section defines correction to maximum dry density to take into account aggregate particles larger than 4.75 mm.

## REFERENCES

### American Society for Testing and Materials (ASTM)

#### ASTM C127-88, Standard Test Method for Specific Gravity and Absorption of Coarse Aggregate.

#### ASTM D698, Standard Test Methods for Laboratory Compaction Characteristics of Soil Using Standard Effort (12,400 ft-lbf/ft³) (600kN-m/m³).

#### ASTM D1557, Test Method for Laboratory Compaction Characteristics of Soil Using Modified Effort (56,000 ft-lbf/ft³).

#### ASTM D4253, Standard Test Methods for Maximum Index Density and Unit Weight of Soils Using a Vibratory Table.

## DEFINITIONS

### Corrected maximum dry density is defined as:

#### D =(D1xD2)(F1 x D2) + (F2 x D1)

#### Where: D = corrected maximum dry density kg/m3.

##### F1 = fraction (decimal) of total field sample passing 4.75 mm sieve.

##### F2 = fraction (decimal) of total field sample retained on 4.75 mm sieve (equal to 1.00 - F1)

##### D1 = maximum dry density, kg/m3of material passing 4.75 mm sieve determined in accordance with Method A C of ASTM D698.

##### D2 = bulk density, kg/m3, of material retained on 4.75 mm sieve, equal to 1000G where G is bulk specific gravity (dry basis) of material when tested to ASTM C127.

#### For free draining aggregates, determine D1 (maximum dry density) to ASTM D4253, dry method when directed by Owner’s Representative.

# PRODUCTS (NOT APPLICABLE)

# EXECUTION (NOT APPLICABLE)

END OF SECTION