# General

## Related Sections

### Section 31 23 33.01 - Excavating, Trenching and Backfilling.

## REFERENCES

### American Society for Testing and Materials (ASTM)

#### ASTM A313/A313M, Standard Specification for Stainless Spring Wire.

#### ASTM A764, Standard Specification for Metallic Coated Carbon Steel Wire, Coated at Size and Drawn to Size for Mechanical Springs.

### Canadian Standards Association (CSA)

#### CAN/CSA-G164, Hot Dip Galvanizing of Irregularly Shaped Articles.

## MEASUREMENT FOR PAYMENT

### Supply and Installation of gabions will be measured in Lump Sum. Includes excavation and preparation of foundation bed and supply and installation of graded stone fill.

# PRODUCTS

## MATERIALS

### Gabion baskets:

#### Factory fabricated so that sides, ends, lid and internal diaphragms readily assemble at site into rectangular baskets of sizes as indicated.

#### Single unit construction or with joints having strength and flexibility equal to that of mesh.

#### When length exceeds horizontal width, provide diaphragms of same mesh as gabion walls to divide basket into equal cells of length not in excess of horizontal width.

#### Wire mesh gabions:

##### Wire mesh to be uniform hexagonal pattern wire woven in triple twist pattern with openings of approximately 80 x 100 mm and fabricated to be non-ravelling. Perimeter edges of mesh to be securely selvedged so that joints formed by connecting selvedges are as strong as body of mesh.

##### Wire to have following dimensions:

###### Mesh: 3.0 mm diameter.

###### Selvedges: 3.8 mm diameter.

###### Binding: 2.0 mm diameter.

##### Wire: hot dip galvanized with minimum coverage of 260 g/m to CSA G164.

##### Interlocking wire fasteners: galvanized steel to ASTM A 764, finish 1, class 1, type 3.

#### Geogrid gabions:

##### Geogrid mesh to be rigid type, uniform, square pattern, non corrosive, high density polyethylene with inhibitors added to resist deterioration by ultra-violet and heat exposure. Geogrid openings to be 50 x 50 mm.

##### Geogrid to have following mechanical properties: Tensile modulus at 2% elongation: to ANSI/ASTM D638M, modified to manufacturer's recommendations, minimum 290 kN/m. Junction strength: to ANSI/ASTM D 638M, modified to manufacturer's recommendations, minimum 90% of single rib strength.

### Gabion mats:

#### Factory fabricated so that sides, ends, lid and internal diaphragms readily assemble at site into rectangular mats.

#### Single unit construction or with joints having strength and flexibility equal to that of mesh.

#### When length exceeds horizontal width, provide diaphragms of same mesh as gabion walls to divide mat into equal cells not in excess of 1 m x 3 m.

#### Wire mesh gabion mats:

##### Wire mesh to be uniform hexagonal pattern wire woven in triple twist pattern with openings of approximately 80 x 100 mm and fabricated to be non ravelling. Perimeter edges of mesh to be securely selvedged so that joints formed by connecting selvedges are as strong as body of mesh.

##### Wire to have following dimensions:

###### Mesh: 2.20 mm diameter.

###### Selvedges: 2.65 mm diameter.

###### Binding: 2.20 mm diameter.

##### Wire: hot dip galvanized with minimum coverage of 260 g/m to CAN/CSA-G164.

##### Interlocking wire fasteners: galvanized steel to ASTM A 764, finish 1 class 1, type 3.

#### Geogrid gabion mats:

##### Geogrid mesh to be rigid type, uniform, square pattern, non corrosive, high density polyethylene with inhibitors added to resist deterioration by ultra-violet and heat exposure. Geogrid opening to be 50 x 50 mm.

##### Geogrid to have following mechanical properties:

###### Tensile modulus at 2% elongation: to ANSI/ASTM D 638M, modified to manufacturer's recommendations, minimum 290 kN/m.

###### Junction strength: to ANSI/ASTM D 638M, modified to manufacturer's recommendations, minimum 90% of single rib strength.

### Stone fill:

#### Hard, durable, abrasion resistant such that it will not disintegrate from action of wetting and drying, wave action, freezing and thawing cycles.

#### Minimum 100 mm to maximum 200 mm dimension for individual stones.

# EXECUTION

## INSTALLATION

### Install gabions to lines and grades as indicated. Follow manufacturer's instructions in assembling baskets.

### Excavate for and backfill behind gabions in accordance with Section 31 23 33.01 – Excavating, Trenching and Backfilling.

## PLACING GABIONS

### Wherever possible, place baskets in position prior to filling with stones.

### Join adjacent baskets together at corners as recommended by manufacturer, so that joints are as strong as mesh.

## FILLING BASKETS AND MATS

### Tension geogrid gabions according to manufacturer's instructions before filling with stone. Do not release wall tension until sufficient stone fill has been placed to prevent wall slackening.

### On exposed faces of gabions, place stones by hand with flattest surfaces bearing against face mesh to produce satisfactory alignment and appearance.

### For wire mesh gabions, fill gabion cells in lifts not exceeding 300 mm and connect opposite walls with 2 tie wires after each lift.

### For geogrid gabions, fill cells in lifts not exceeding 300 mm and connect opposite walls with 2 polyethylene braids after each lift.

END OF SECTION