# GENERAL

## RELATED SECTIONS

### Section 31 05 16 – Aggregates for Earthwork.

### Section 31 23 33.01 - Excavating, Trenching and Backfilling.

### Section 32 11 23 - Aggregate Base Courses.

## REFERENCES

### American Society for Testing and Materials (ASTM).

#### ASTM C117, Standard Test Method for Material Finer Than 0.075 mm Sieve in Mineral Aggregates by Washing.

#### ASTM C136, Standard Test Method for Sieve Analysis of Fine and Coarse Aggregates.

#### ASTM D698, Standard Test Method for Laboratory Compaction Characteristics of Soil Using Standard Effort (12,400 ft-lbf/ft3) (600 kN-m/m3).

#### ASTM D1557, Test Method for Laboratory Compaction Characteristics of Soil Using Modified Effort (56,000 ft-lbf/ft3) (2,700 kN-m/m3).

#### ASTM D4318, Standard Test Methods for Liquid Unit, Plastic Unit and Plasticity Index of Soils.

### Canadian General Standards Board (CGSB).

#### CAN/CGSB-8.1, Sieves, Testing, Woven Wire, Inch series.

#### CAN/CGSB-8.2, Sieves, Testing, Woven Wire, Metric.

# PRODUCTS

## MATERIALS

### Granular sub-base material to Section 31 05 16 – Aggregates for Earthwork and following requirements:

#### Crushed pit run or screened stone, gravel or sand.

#### Granulations to be within limits specified when tested to ASTM C136 and ASTM C117 - sieve sizes to CAN/CGSB-8.1.

##### Granulation to:

Sieve Designation                       	% Passing (Base Type 2)

100 mm						-

75 mm						-

50 mm					     75-100

38.1 mm						-

25 mm						-

19 mm						-

15.9 mm				   	      45-80

12.5 mm						-

9.5 mm						-

4.75 mm				   	      25-55

2.00 mm						-

1.20 mm				   	      12-35

0.425 mm						-

0.180 mm						-

0.075 mm				     	         3-6

#### Other properties as follows:

##### Liquid limit:  to ASTM D4318, maximum 25

##### Plasticity index:  to ASTM D4318, maximum 6

# EXECUTION

## PLACING

### Place granular sub-base after subgrade is inspected and approved by Owner.

### Construct granular sub-base to depth and grade in areas indicated.

### Ensure no frozen material is placed.

### Place material only on clean unfrozen surface, free from snow or ice.

### Place granular sub-base materials using methods which do not lead to segregation or degradation.

### Place material to full width in uniform layers not exceeding 150 mm compacted thickness. Owner may authorize thicker lifts (layers) if specified compaction can be achieved.

### Shape each layer to smooth contour and compact to specified density before succeeding layer is placed.

### Remove and replace portion of layer in which material has become segregated during spreading.

## COMPACTION

### Compaction equipment to be capable of obtaining required material densities.

### Compact to density of not less than 98% corrected maximum dry density ASTM D698.

### Shape and roll alternately to obtain smooth, even and uniformly compacted sub-base.

### Apply water as necessary during compaction to obtain specified density.

### In areas not accessible to rolling equipment, compact to specified density with mechanical tampers approved by Owner.

### Correct surface irregularities by loosening and adding or removing material until surface is within specified tolerance.

## SITE TOLERANCES

### Finished sub-base surface to be within 10 mm of elevation as indicated but not uniformly high or low.

## PROTECTION

### Maintain finished sub-base in condition conforming to this section until succeeding base is constructed, or until granular sub-base is accepted by Owner.

END OF SECTION