# GENERAL

## SECTION INCLUDES

### Materials and installation for asphalt concrete pavement for car park areas, driveways to buildings, and walks or play areas.

## RELATED SECTIONS

### Section 01 33 00 – Submittal Procedures.

### Section 01 45 00 – Quality Control.

### Section 31 05 16 – Aggregates for Earthworks.

### Section 31 23 33.01 – Excavating, Trenching and Backfilling.

### Section 32 16 15 – Concrete Walks, Curbs and Gutters.

### Section 32 17 23 – Pavement Marking.

## REFERENCES

### Canadian General Standards Board (CGSB)

#### CAN/CGSB-8.1, Sieves Testing, Woven Wire, Inch Series.

#### CAN/CGSB-8.2, Sieves Testing, Woven Wire, Metric.

#### CAN/CGSB-16.1, Cutback Asphalts for Road Purposes.

### American Association of State Highway and Transportation Officials (AASHTO)

#### AASHTO M320 - Standard Specification for Performance Grade Asphalt Binder.

### American Society for Testing and Materials International, (ASTM)

#### ASTM C88, Standard Test Method for Soundness of Aggregates by Use of Sodium Sulphate or Magnesium Sulphate.

#### ASTM C117, Standard Test Method for Material Finer Than 0.075 mm (No. 200) Sieve in Mineral Aggregates by Washing.

#### ASTM C123, Standard Test Method for Lightweight Particles in Aggregate.

#### ASTM C127, Standard Test Method for Density, Relative Density (Specific Gravity), and Absorption of Coarse Aggregate.

#### ASTM C128, Standard Test Method for Density, Relative Density (Specific Gravity), and Absorption of Fine Aggregate.

#### ASTM C131, Standard Test Method for Resistance to Degradation of Small-Size Coarse Aggregate by Abrasion and Impact in the Los Angeles Machine.

#### ASTM C136, Standard Method for Sieve Analysis of Fine and Coarse Aggregates.

#### ASTM D698, Standard Test Method for Laboratory Compaction Characteristics of Soil Using Standard Effort (12,400 ft-lbf/ft3) (600 kN-m/m3).

#### ASTM D977 – Standard Specification for Emulsified Asphalt.

#### ASTM D995, Standard Specification for Requirements Mixing Plants for Hot-Mixed, Hot-Laid Bituminous Paving Mixtures.

#### ASTM D2419, Standard Test Method for Sand Equivalent Value of Soils and Fine Aggregate.

#### ASTM D3203, Standard Test Method for Percent Air Voids in Compacted Dense and Open Bituminous Paving Mixtures.

#### ASTM D4318, Standard Test Method for Liquid Limit, Plastic Limit and Plasticity Index of Soils.

#### ASTM D4791, Standard Test Method for Flat Particles or Elongated Particles in Coarse Aggregate.

### Asphalt Institute (AI)

#### Asphalt Institute MS-2-1993 Sixth Edition, Mix Design Methods for Asphalt Concrete.

## SUBMITTALS

### Submit asphalt concrete mix design to Owner for approval.

### Materials to be tested by testing laboratory approved by Owner.

### Submit test certificates showing suitability of materials at least 4 weeks prior to commencing work.

### Inform Owner of proposed source of aggregates and provide access for sampling at least 4 weeks prior to commencing work.

# PRODUCTS

## MATERIALS

### Granular base and sub-base material: to Section 31 05 16 – Aggregates for Earthwork and following requirements:

#### Crushed or screened stone, gravel or sand.

#### Gradations: within limits specified when tested to ASTM C136 and ASTM C117. Sieve sizes to CAN/CGSB-8.1.

#### Table:

| Sieve Designation | Granular Base | Granular Sub-Base |
| --- | --- | --- |
| 200 mm | - | - |
| 75 mm | - | - |
| 50 mm | - | 75-100 |
| 38.1 m | - | - |
| 25 mm | - | - |
| 19 mm | 100 | - |
| 15.9 mm | - | 45-80 |
| 12.5 mm | - | - |
| 9.5 mm | 55-80 | - |
| 4.75 mm | 35-60 | 25-55 |
| 2.00 mm | - | - |
| 1.20 mm | 17-35 | 12-35 |
| 0.425 mm | - | - |
| 0.180 mm | - | - |
| 0.075 mm | 3-6 | 3-6 |

#### Granular base aggregates:

##### Crushed particles: at least 50 % of particles by mass retained on 4.75 mm sieve to have at least 1 freshly fractured face.

### Asphalt concrete aggregates:

#### Coarse aggregate is aggregate retained on 4.75 mm sieve and fine aggregate is aggregate passing 4.75 mm sieve when tested to ASTM C117.

#### When dryer drum plant or plant without hot screening is used, process fine aggregate through 4.75 mm sieve and stockpile separately from coarse aggregate.

#### Separate stock piles for coarse and fine aggregate are not required for sheet asphalt.

#### Do not use aggregates having known polishing characteristics in mixes for surface courses.

#### Aggregate: material to Section 31 05 16 – Aggregates for Earthwork and following requirements:

##### Crushed stone or gravel.

##### Gradations to be within limits specified when tested to ASTM C136 and ASTM C117, Latest Edition. Sieve sizes to CAN/CGSB-8.1, Latest Edition.

| Sieve Designation (Type 1) Base | % Passing (Base Type 2) |
| --- | --- |
| 19.0 mm | 100 |
| 9.5 mm | 60-80 |
| 4.75 mm | 40-65 |
| 2.00 mm | 30-50 |
| 0.180 mm | 5-20 |
| 0.075 mm | 3-8 |

##### Sand equivalent: to ASTM D2419, Minimum 50.

##### Magnesium Sulphate soundness: to ASTM C88. Max % loss by weight: coarse aggregate 12, fine aggregate 16.

##### Los Angeles Degradation: to ASTM C131, Max % loss by weight: coarse aggregate, 35.

##### Absorption: to ASTM C127, Max % by weight: coarse aggregate, 1.75.

##### Lightweight particles: to ASTM C123, Max % by mass, with less than 1.95. Relative density (formally Specific Gravity): 1.5.

##### Flat and elongated particles: to ASTM D4791, (with length to thickness ratio greater than 5): Max % by weight: coarse aggregate, 15.

##### Crushed particles: at least 60 % of particles by mass within each of following sieve designation ranges to have at least 1 freshly fractured face. Material to be divided into ranges using methods of ASTM C136,

| Passing |  | Retained on |
| --- | --- | --- |
| 19 mm | to | 9.5 mm |
| 9.5 mm | to | 4.75 mm |

##### Regardless of compliance with specified physical requirements, fine aggregates may be accepted or rejected on basis of past field performance.

### Mineral filler for asphalt concrete:

#### Finely ground particles of limestone, hydrated lime, Portland cement or other approved non-plastic mineral matter, thoroughly dry and free from lumps.

#### Add mineral filler when necessary to meet job mix aggregate gradation or as directed by Owner to improve mix properties.

### Asphalt cement: to AASHTO M320.

### Asphalt Prime: to ASTM D997.

### Sand blotter: clean granular material passing 4.75 mm sieve and free from organic matter or other deleterious materials.

### Asphalt tack coat: to ASTM D977.

## MIX DESIGN

### Job mix formula to be approved by Owner.

### Design of mix: by Marshall method to requirements below:

#### Compaction blows on each face of test specimens: 50.

#### Mix physical requirements:

| Property | Asphalt / Concrete |
| --- | --- |
| Marshall Stability at 60˚kN minimum | 5.5 |
| Flow Value, mm. | 2 - 4 |
| Air Voids in Mixture, % | 3 - 5 |
| Voids in Mineral Aggregate, % minimum | 15 |
| Index of Retained Stability, % minimum | 75 |

#### Measure physical requirements as follows:

##### Marshall load and flow value.

##### Compute void properties on basis of bulk specific gravity of aggregate to ASTM C127, and ASTM C128. Make allowance for volume of asphalt absorbed into pores of aggregate.

##### Air voids: to ASTM D3203.

##### Voids in mineral aggregate: to Asphalt Institute, MS-2 chapter 4.

##### Index of Retained Stability.

#### Do not change job-mix without prior approval of Owner. When change in material source proposed, new job-mix formula to be approved by Owner.

#### Return plant dust collected during processing to mix in quantities acceptable to Owner.

## EQUIPMENT

### Pavers: mechanical grade controlled self-powered pavers capable of spreading mix within specified tolerances, true to line, grade and crown indicated.

### Rollers: sufficient number of rollers of type and weight to obtain specified density of compacted mix.

### Vibratory rollers for parking lots and driveway:

#### Minimum drum diameter: 750mm.

#### Maximum amplitude of vibration (machine setting): 0.5mm for lifts less than 40mm thick.

### Haul trucks: of sufficient number and of adequate size, speed and condition to ensure orderly and continuous operation and as follows:

#### Boxes with tight metal bottoms.

#### Covers of sufficient size and weight to completely cover and protect asphalt mix when truck fully loaded.

#### In cool weather or for long hauls, insulate entire contact area of each truck box.

### Suitable hand tools

# EXECUTION

## SUBGRADE SURFACE PREPARATION AND INSPECTION

### Verify grades of subgrade drains and other items set in paving area for conformity with elevations and sections before placing granular base material.

### Obtain approval of subgrade by Owner before placing granular base.

## GRANULAR BASE AND GRANULAR SUBBASE

### Place granular base and sub-base material on clean unfrozen surface, free from snow and ice.

### Place granular base and sub-base to compacted thicknesses as indicated. Do not place frozen material.

### Place in layers not exceeding 150 mm compacted thickness. Compact to density not less than 98 % maximum dry density in accordance with ASTM D698.

### Finished base surface to be within 10 mm of specified grade, but not uniformly high or low.

## ASPHALT PRIME

### Emulsified asphalt:

#### Dilute asphalt emulsion with clean water at 1:1 ratio for application. Mix thoroughly by pumping or other method approved by Owner.

#### Apply diluted asphalt emulsion at rate directed by Owner but do not exceed 5 L/m2.

#### Apply on damp surface unless otherwise directed by Owner.

### Do not apply prime when air temperature is less than 5˚C or when rain is forecast within 2 hours.

### If asphalt prime fails to set within 24 hours, spread sand blotter material in amounts required to absorb excess material. Sweep and remove excess blotter material.

## PLANT AND MIXING REQUIREMENTS

### To ASTM D995.

## ASPHALT CONCRETE PAVING

### Obtain approval of primer from Owner before placing asphalt mix.

### Place asphalt mix only when base or previous course is dry and air temperature is above 5˚C.

### Place asphalt concrete in compacted layers not exceeding 50 mm.

### Minimum 135˚C mix temperature required when spreading.

### Maximum 160˚C mix temperature permitted at any time.

### Compact each course with roller as soon as it can support roller weight without undue cracking or displacement.

### Compact parking lot and driveway asphalt concrete to density not less than 95 % of density obtained with Marshall specimens prepared in accordance with ASTM D1559, ion from samples of mix being used. Roll until roller marks are eliminated.

### Keep roller speed slow enough to avoid mix displacement and do not stop roller on fresh pavement.

### Moisten roller wheels with water to prevent pick up of material.

### Compact mix with hot tampers or other equipment approved by Owner in areas inaccessible to roller.

### Finish surface to be within 10 mm of design elevation and with no irregularities greater than 10 mm in 4.5 m.

### Repair areas showing checking, rippling or segregation as directed by Owner.

## JOINTS

### Remove surplus material from surface of previously laid strip. Do not deposit on surface of freshly laid strip.

### Paint contact surfaces of existing structures such as manholes, curbs or gutters with bituminous material prior to placing adjacent pavement.

### For cold joints, cut back to full depth vertical face and tack face with hot asphalt.

### For longitudinal joints, overlap previously laid strip with spreader by 25 to 50 mm.

## TESTING

### Inspection and testing of asphalt pavement will be carried out by designated testing laboratory. Refer to Sections 01 29 83 – Payment Procedures for Testing Laboratory Services and Section 01 45 00 - Quality Control.

### Costs of tests will be paid under Section 01 21 00 – Allowances.

## PROTECTION

### Keep vehicular traffic off newly paved areas until paving surface temperature has cooled below 38˚C. Do not permit stationary loads on pavement until 24 hours after placement.

### Provide access to buildings as required. Arrange paving schedule so as not to interfere with normal use of premises.

END OF SECTION