# GENERAL

## REFERENCES

#### Master Painters Institute (MPI)

##### Architectural Painting Specification Manual, MPI #32 Traffic Markings Paint, Alkyd.

#### South Coast Air Quality Management District (SCAQMD)

##### SCAQMD Rule 1113, Architectural Coatings.

## SUBMITTALS

### Submit to Owner following material sample quantities at least 4weeks prior to commencing work.

#### Two 1L samples of each type of paint.

### Mark samples with name of project and its location, paint manufacturer's name and address, name of paint, CGSB specification number and formulation number and batch number.

# PRODUCTS

## MATERIALS

### Paint and Markings:

#### To MPI #32, Alkyd zone/traffic marking.

#### Traffic Marking Coatings: maximum VOC limit 450 g/L to SOR/2009-264 Schedule 1, to SCAQMD Rule 1113.

#### In accordance with MPI recommendation for surface conditions.

### Thinner: to MPI listed manufacturer.

# Execution

## EQUIPMENT REQUIREMENTS

### Paint applicator to be an approved pressure type mobile distributor capable of applying paint in single, double and dashed lines. Applicator to be capable of applying marking components uniformly, at rates specified, and to dimensions as indicated, and to have positive shut-off.

## CONDITION OF SURFACES

### Pavement surface to be dry, free from ponded water, frost, ice, dust, oil, grease and other foreign materials.

## APPLICATION

### Lay out pavement markings as indicated on drawings.

### Unless otherwise approved by Owner, apply paint only when air temperature is above 10° C, wind speed is less than 60km/h and no rain is forecast within next 4 h.

### Apply traffic paint evenly at rate of 3 m2/L.

### Do not thin paint unless approved by Owner.

### Symbols and letters to conform to dimensions indicated.

### Paint lines to be of uniform colour and density with sharp edges.

### Thoroughly clean distributor tank before refilling with paint of different colour.

## TOLERANCE

### Paint markings to be within plus or minus 12 mm of dimensions indicated.

## PROTECTION OF COMPLETED WORK

### Protect pavement markings until dry.

END OF SECTION